Exploring Two-Dimensional Electron Systems at Extreme Magnetic Fields

with Optical and Terahertz 2DFT Spectroscopy

Karaiskaj, D. (University of South Florida, Physics); Hilton, D. (University of Alabama, Birmingham, Physics) and Shan, J. (Pennsylvania State University, Physics)

Introduction

The main objective of this proposal is the investigation of the fundamental many-body interactions at nanoscale of two-dimensional electron and hole gases at high magnetic fields. The main experimental goal in the proposed work is to perform coherent four-wave mixing (FWM) experiments systematically on the GaAs/AlGaAs and transition-metal dichalcogenides (TMD) materials. We have built a state-of-the-art instrument which resides at the NHMFL and can perform two-dimensional Fourier transform (2DFT) spectroscopy based on the coherent FWM signal at extreme magnetic fields up to 25 Tesla.

Experimental

We have measured 2DFT spectra from one undoped and one modulation doped GaAs/AlGaAs quantum well at different magnetic fields from zero to 10 Tesla. We have performed preliminary absorption measurements up to 20 Tesla which are not shown here. We also collected preliminary data on MoS2 up to 20 Tesla. The measurements were taken in cell 1 and 5.

Results and Discussion

We found interesting differences between Landau levels in the undoped and doped quantum wells. The Landau levels in the undoped quantum well (Fig. 1) show vertical elongation which are absent Landau levels in (Fig. 2) the modulation doped quantum well. In collaboration with theorists we are performing simulations in order to understand this effect.

Conclusions

Striking differences between Landau levels in doped and undoped samples were observed.

Acknowledgements

A portion of this work was performed at the National High Magnetic Field Laboratory, which is supported by National Science Foundation Cooperative Agreement No. DMR-1157490 and the State of Florida. In addition, the work on GaAs/AlGaAs 2D electron gases is supported by NSF DMR-1409473 whereas the work on TMDs is supported by the DOE, Office of Basic Energy Sciences, Division of Materials Sciences and Engineering under Award DE-SC0012635.

# Text boxes

Fig.2 2DFT spectra from a modulation doped quantum well. Left LL1 and right LL0 are shown at three different magnetic fields.

Fig.1 2DFT spectra from an undoped quantum well. (a-b) Landau levels at 6.5 T and 10 T respectively. (c-d) The excitonic region at the same fields.