Record Zero-Field Splitting in a Polymeric Chain Containing Six-Coordinate Ni(II) Ions

Manson, J.L. (Eastern Washington U., Chemistry); Blackmore, W.J.A.; Brambleby, J.; Goddard, P.A. (U. Warwick, UK, Physics) and Ozarowski, A. (NHMFL, Tallahassee)

Introduction

While much attention has been paid to low-dimensional antiferromagnetic S = 1 Ni(II) coordination polymers, challenges persist in extracting the anisotropy parameters D and E of such compounds, especially when magnetic interactions (J) co-exist [1,2]. To this end, we have designed a molecule-based coordination polymer that exhibits negligible J, thus facilitating determination of D and E by high-field/frequency ESR [3]. The tetragonal compound, Ni(SiF6)(vinim)4 (vinim = 1-vinylimidazole) [4], forms parallel 1D Ni-F-Si-F-Ni chains with large interchain spacings ensured by bulky vinim ligands (Fig. 1a). Near-octahedral NiN4F2 sites exhibit Ni-N and Ni-F bond lengths of 2.06 and 2.10 Å, respectively. It serves as a basis for which to compare parameters against more complicated examples such as [Ni(HF2)(pyz)2]SbF6 (pyz = pyrazine) that has Ni-F-H-F-Ni chains and J1D ~ D ~ TN [1].

Experiment Details

High-field, high-frequency ESR spectra at temperatures ranging from 5 to 20 K were recorded on a home-built spectrometer at the EMR facility of the NHMFL, Tallahassee, with the microwave frequencies ν = 197 ( 658 GHz. The instrument is a transmission-type device and uses no resonance cavity. The microwaves were generated by a phase-locked Virginia Diodes source, generating frequency of 13(1) GHz, and equipped with a cascade of frequency multipliers to generate higher harmonic frequencies. An Oxford Instruments superconducting magnet capable of reaching a field of 17 T was employed.

Results and Discussion

Continuous-wave ESR spectra recorded on a powder sample of Ni(SiF6)(1-vinim)4 are shown in Fig. 1b along with a simulation (red) based on the Hamiltonian:

Ĥ = BB {g} Ŝ + D { Ŝz2 – S(S+1)/3 } + E ( Ŝx2 – Ŝy2)                [1]

The simulations gave an anisotropic g-matrix with gx = gy = 2.26, gz = 2.15, and D = +14 cm(1. The simulation captures the majority of resonances as shown collectively in Fig. 2. The values of g and D are also consistent with susceptibility and magnetization measurements. A positive-D denotes easy-plane anisotropy with ms = 0 being the ground state. While a large negative-D value of –22.3 cm(1 has been found in Ni(CH3CO2)2(im)4 (im = imidazole) [5], the D found for Ni(SiF6)(vinim)4 is the largest positive-value observed thus far. Notably, a tetrahedral NiSe4 coordination complex features D = +45 cm-1 [6]. We attribute the large-D to a stark difference in orbital reduction factors for ionic SiF62- as compared to coordinate covalent vinim ligands. Combined with a very small intrachain J, the enormous D/J ratio puts this material well inside the so-called large-D (i.e., quantum paramagnetic) phase [7].

Acknowledgements

Work at EWU was supported by the NSF under grant no. DMR-1306158. This work was performed at the National High Magnetic Field Laboratory, which is supported by NSF Cooperative Agreement No. DMR-1157490 and the State of Florida. WJAB, JB and PAG acknowledge the EPSRC for funding.

References

[1]	Manson, J.L., et al., Inorg. Chem. 50, 5990 (2011).

[2] 	Manson, J.L., et al., Dalton Trans. 41, 7235 (2012).

[3]	Krzystek, J., et al., Coord. Chem. Rev. 250, 2308 (2006).

[4]	Manson, J.L., et al., to be published.

[5]	Boča, R., et al., Chem. Phys. Lett. 373, 402 (2003).

[6]  Jiang, S.-D., et al., J. Am. Chem. Soc., 137, 12923-12928 (2015).

[7]	Wierschem, K., et al., P. Mod. Phys. Lett. B 28, 1430017 (2014).

# Text boxes

Fig. 1. (a) 1D chain and (b) transmission

ESR spectra for Ni(SiF6)(vinim)4 at 5 K.

(a)

Si

F

Ni

C

N

c

(b)

Fig.2 Resonance field vs. frequency dependence for Ni(SiF6)(vinim)4 obtained at 5 K.