High Field EPR Study of Catalytically Active Polyoxometalates [Cu(H2O)(TiO)2(AsW9O33)2]12-

Bindra, J.K.; Diefenbach, K. (FSU, Chemistry); van Tol, J. (NHMFL); Dalal N.S. (NHMFL & FSU, Chemistry) and Kortz, U. (Jacobs U., Bremen, Germany, School of Engineering and Science)

Introduction

The goal of this study was to examine the use of HFEPR to characterize the family of polyoxometalates  [TMII(H2O)(TiO)2(AsW9O33)2]12( (TM = Co, Ni, Cu), Fig. 1. Because of their catalytic and biochemical applications, these polyoxometalates (POMs) have recently gained interest.1 All three POMs are isostructural, composed of two [AsW9O33]9( building blocks connected by two penta-coordinated Ti4+ ions and one penta-coordinated TM2+ ion. To augment the x-ray and optical and electrochemical studies high-field electron paramagnetic resonance spectroscopy (HF-EPR) was used to characterize their electronic ground state and related magnetic properties.2

Experimental

All three POMs were synthesized by the Kortz group at Jacobs University. X-band (9.8 GHz) powder EPR spectra were measured using a Bruker Elexsys 500 spectrometer available at FSU Chemistry Department. Variable temperature HF-EPR powder spectra at 240 GHz were measured using a heterodyne spectrometer employing a 12.5 T superconducting magnet at NHMFL. Variable temperatures from 4 to 295 K were achieved using an Oxford cryostat.

Results and Discussion

Fig. 2 shows some typical EPR spectra of the Cu- POM at X band (9.8 GHz) (2a) and at high frequency (240 GHz) (2b). The X-band spectrum indicated anisotropic environment. The 240 GHz spectrum (Fig. 2b) is characteristic of Cu2+ (S = 1/2) in a rhombic local environment. HF-EPR is an invaluable tool essential for studying these novel materials. Similar systematic data have been obtained on several related compounds; detailed analysis is in progress.

Conclusions

This study once again demonstrates how the high spectral resolution afforded by HF-EPR enables detection of the finer features in the electronic structure and bonding geometry of a large paramagnetic POM complex such as Cu-POM.

Acknowledgements

This work was performed at the National High Magnetic Field Laboratory, which is supported by National Science Foundation Cooperative Agreement No. DMR-1157490 and the State of Florida.

References

[1]	Kortz, U., et al., Coord. Chem. Rev., 253, 2315–2327 (2009).

[2]	Kortz, U., et al., Inorg. Chem., 43 (7), 2308–2317 (2004).

# Text boxes

Fig. 1. Crystal structure of

Co-POM.

a

b

Fig. 2. X-Band (a) and 240 GHz (b) spectra

of Cu-POM.