Giant Magneto-Resistance in Epitaxial (La0.7Sr0.3MnO3)0.5: (ZnO)0.5 Nanocomposites

Pan, W. (Sandia National Labs); Jiang, Y.X. (NHMFL and Georgia Institute of Technology); Ihlefeld, J. (SNL); Lu, P. (SNL) and Lee, S.R. (SNL)

Introduction

A great deal of research has been carried out in oxide material systems [1]. Among them, ZnO and La0.7Sr0.3MnO3 (LSMO) are of particular interest due to their superb optical properties and colossal magneto-resistive effect. Here, we report our recent results of magneto-transport studies in self-assembled, epitaxial (ZnO)0.5:(La0.7Sr0.3MnO3)0.5 nanocomposite films [1].

Experimental

The epitaxial LSMO (70%)-ZnO (30%) phase-separated nanocomposites were prepared by rf magnetron sputtering on (001) LaAlO3 single crystalline substrates. Electronic measurements of the transport properties were performed in a VTI cryostat in SCM2. Silver epoxy was used for making ohmic contacts to our oxide nanostructure samples.

Results and Discussion

The epitaxial LSMO (70%)-ZnO (30%) phase-separated nanocomposites were prepared by rf magnetron sputtering on (001) LaAlO3 single crystalline substrates. X-ray diffraction analysis showed that the LSMO phase was cube-on-cube epitaxial on the substrate and the ZnO phase possessed a 11-20 texture. AC-STEM imaging and EDS chemical mapping were used to characterize these ZnO/LSMO composite films. Compositional analysis indicates mutual solubility between ZnO and LSMO, and compositional variation across the ZnO/LSMO interfaces. In our magneto-transport studies, a giant negative magneto-resistance was observed at low temperatures and high magnetic fields, reaching almost 700% at a magnetic field of 5 Tesla at 70K. This giant magneto-resistance decreases with increasing temperatures, to ~ 15% at 200K.  We believe that this giant magneto-resistance is related to multiple-orientated ZnO pillars and a tree-like 3D morphology in our ZnO/LSMO nanocomposites.

Conclusions

Our results show that epitaxial (La0.7Sr0.3MnO3)0.5: (ZnO)0.5 nanocomposites are promising candidates for giant magneto-resistance applications, and may have import implications in spin transport properties in our ZnO/LSMO composite films.

Acknowledgements

This work was supported by a Laboratory Directed Research and Development project at Sandia National Laboratories. Sandia is a multiprogram laboratory managed and operated by Sandia Corporation, a wholly owned subsidiary of Lockheed Martin Corporation, for the U.S. Department of Energy’s National Nuclear Security Administration under contract DE-AC04-94AL85000. We thank Glover Jones and Hongwoo Baek for help. A portion of this work was performed at the National High Magnetic Field Laboratory, which is supported by National Science Foundation Cooperative Agreement No. DMR-1157490 and the State of Florida.

References

[1] J. Mannhart and D.G. Schlom, Science 327, 1607 (2010).

# Text boxes

Left: XRD results for a 100 nm thick film on 001-oriented SrTiO3.  * denotes the 001-SrTiO3 peaks. Distinct LSMO and ZnO peaks are also shown.

Right: AC-STEM imaging is used to characterize the ZnO/LSMO composite films grown on STO and LAO substrates. The results show that the ZnO/LSMO films can be grown epitaxially on both substrates but microstructures of the films are highly dependent of the substrate used, and overall film composition, and growth temperatures.

Magneto-resistance measurements in one film of 70%LSMO and 30%ZnO prepared on (001) LAO substrate.  A giant magneto-resistance was observed.