Discovery of a Magnetic Topological Semimetal Sr1-yMn1-zSb2

Liu, J.Y.; Hu, J.; Mao, Z.Q. (Tulane U. Physics); Radmanesh, S.M.A.; Spinu, L. (UNO, Physics); Graf, D. (NHMFL) and Chiorescu, I. (NHMFL & FSU, Physics)

Introduction

Weyl semimetals evolve from Dirac semimetals in the presence of breaking spatial inversion symmetry (IS) or time reversal symmetry (TRS). Recent discoveries of IS-breaking Weyl semimetals in monopnictides [1-2] and photonic crystals [3] have generated immense interests. We have recently discovered a new type of magnetic topological semimetal phase arising from 2D Sb layers in Sr1-yMn1-zSb2. The combination of relativistic fermion behavior and ferromagnetism make it a promising candidate for exploring the long-sought TRS -breaking Weyl semimetals [4].

Experimental

The Sr1-yMn1-zSb2 (y, z < 0.1) single crystals were synthesized using the self-flux method with the stoichiometric mixture of Sr, Mn and Sb elements. The high field magnetoresistance and Hall effect measurements were performed using the 31T resistive magnet in the DC field facility at NHMFL.

Results and Discussion

We have measured the quantum transport properties of Sr1-yMn1-zSb2 single crystals with ferromagnetic properties [4]. Very strong Shubnikov-de Hass (SdH) oscillations in both Magneto- and Hall resistivity measurements have been observed (Fig. 1b), with an oscillation frequency ~ 67T which corresponds to a small  Fermi surface. The oscillation frequency follows a 1/cosθ dependence with field orientation, suggesting a quasi-2D Fermi surface that is consistent with the 2D crystal structure (Fig.1a). The effective mass extracted from the temperature damping of oscillation amplitude is as small as 0.14m0. From the Landau level index fan diagram (Fig. 1c) constructed from the conductivity oscillation (Fig. 1c, inset), a Berry phase close to π can be extracted. These characteristics are consistent with 2D relativistic fermion systems.

Conclusions

We have demonstrated that Sr1-yMn1-zSb2 hosts relativistic fermions from quantum transport property measurements. Given that Sr1-yMn1-zSb2 exhibits ferromagnetism up to 400K, it provides the first example of magnetic topological semimetal and offers a wonderful opportunity to seek the long-sought magnetic Weyl state and investigate the coupling of Dirac/Weyl fermions with magnetism.

Acknowledgements

A portion of this work was performed at the NHMFL, which is supported by NSF Cooperative Agreement No. DMR-1157490 and the State of Florida. The work at Tulane University was supported by the NSF (DMR-1205469) and Louisiana Board of Regents. The work at UNO is supported by the NSF under the NSF EPSCoR (EPS-1003897) and Louisiana Board of Regents. The work at FSU and at the National High Magnetic Field Laboratory is also partially supported by NSF grant No. DMR-1206267 and DOE DE-NA0001979 grant.

References

[1]	S-M. Huang, et al, Nature Commun. 6, 7373 (2015).

[2]	H. Weng, et al, Phys. Rev. X 5, 011029, (2015).

[3]	L. Lu, et al, Science 349, 622-624, (2015).

[4]	J.Y. Liu, et al, preprint at arXiv:1507.07978, submitted to Nature Materials, in revision.

# Text boxes

Fig.1 a, Crystal structure of Sr1-yMn1-zSb2. b, SdH oscillations in Magneto- and Hall resistivity at various temperatures. c, the Landau Level index fan diagram derived from the conductivity oscillations shown in inset. The linear fit yields an intercept value of 0.46, consistent with a π Berry phase expected for a relativistic system.