Development of a Gas Plasma-Based THz Time-Domain Spectrometer for the 25 T Florida Split Helix Magnet System

Curtis, J.A. (UAB, Physics) ; Barman, B. (UAB, Physics) ; Tokumoto , T.D. (UAB, Physics) ; McClintock, L.M. (UAB, Physics) ; Reno, J. (SNL) ; Karaiskaj,D. (USF, Physics) ; McGill, S.A. (FSU, NHMFL) and Hilton, D.J. (UAB, Physics)

Introduction

THz time-domain spectroscopy, an ultrafast free-space optical technique at THz frequencies (0.1-15 THz), has been used in recent years in magneto optical configurations to study many interesting material systems including two dimensional electron gasses [1] and two dimensional hole gasses [2].

Experimental

In order to extend the magnetic field range of these measurements we have developed a gas plasma-based THz time-domain spectrometer (TTDS) for use in the 25 T Florida Split Helix magnet system at the National High Magnetic Field Laboratory at Florida State University. The experimental setup is shown in Fig. 1. We have demonstrated that this system is sensitive to THz frequencies in excess of 15 THz in the absence of sample probe and magnet windows. Fig. 2 shows the time-domain signal and calculated spectrum.

Results and Discussion

We have recently performed the first high-field TTDS measurements in this magnet system up to 25 T. A high mobility (μ=3.6 x 106cm2V-1s-1) GaAs two dimensional electron gas was chosen as a test sample due to its well-known effective mass, which corresponds to a cyclotron frequency well within the expected bandwidth of the system. Fig. 3 shows the transmitted THz electric field through the sample with the calculated spectra for 6 magnetic fields (0-25 T).

Conclusion

The limited bandwidth, which is currently under investigation, is the initial experimental validation that we can perform subpicosecond terahertz characterization using this custom designed spectrometer.

Acknowledgements

A portion of this work was performed at the National High Magnetic Field Laboratory, which is supported by National Science Foundation Cooperative Agreement No. DMR-1157490 and the State of Florida. A portion of this work is supported by the National Science Foundation under Grant Nos. DMR-1056827 (JAC, TT, and DJH), DMR-1229217 (SAM and DJH), DMR-1409473 (DK).

References

[1] Q. Zhang et al, Phys. Rev. Lett. 113, 047601 (2014).

[2] N. Kamaraju et al, Appl. Phys. Lett. 106, 031902 (2015).

# Text boxes

Fig. 1 A gas plasma based THz time-domain spectrometer with Split Helix magnet system.

Fig. 2 Transmitted THz electric field and calculated spectrum through Split Helix without magnet windows and probe.

Fig 3. Transmitted THz electric field and calculated spectrum through GaAs high mobility 2DEG inside Split Helix.