Field-Induced Lifshitz Transition in the Intermediate Valence State of -YbAlB4

Shimura, Y.; Nakatsuji, S. (Institute for Solid State Physics, University of Tokyo), Zeng, B.; Zhang, Q. and Balicas, L. (NHMFL, FSU)

Introduction

-YbAlB4 has a strongly intermediate valence state between Yb2+ and Yb3+ below Tv ~ 200 K.  In the typical intermediate valence system, the Fermi liquid ground state becomes stable and no instability is expected below Tv. By contrast, -YbAlB4 exhibits a different characteristic temperature dependence which implies the formation of a heavy fermion state between 30 - 40 K and again at 8 K, even below Tv [1,2]. The quantum phase transition corresponding to these anomalies is also expected from the field dependence at low temperatures.

Experimental

Single crystals of -YbAlB4 were synthesized by an Al self-flux method. The initial ratio of the starting material is Yb:B:Al = 1:4:30 - 600. Magnetoresisitance ( (B)) was measured with temperatures down to 0.36 K and in applied magnetic fields of up to 45 T at the Hybrid magnet facilities. The field direction is mainly parallel to c-axis which is the Ising easy axis.

Results and Discussion

Figure 1 shows the Shubnikov de-Haas oscillation components of the magnetoresistance (SdH) above 25 T. The lower panels indicate the results of the Fast Fourier Transform for SdH for a window of 25 - 33 T (left) and larger field window of 35 - 45 T (right). Evidently, the oscillation with F ~ 900 T is observed only below BM ~ 34 T, suggesting the emergence of the field-induced Lifshitz transition/crossover associated with a change of the Fermi surface. This is only observed for the Ising easy c-axis. In the field BM, the field derivative of Hall resistivity dxy/dB exhibits a minimum, implying the carrier density change.  Normally, while magnetization shows a distinct metamagnetic behavior at BM, the metamagnetic anomaly in -YbAlB4 is very small (less visible) when compared with typical metamagnetic heavy Fermion compounds like YbCu4Ag and CeRu2Si2. Strong valence fluctuation with the higher energy scale Tv ~ 200 K (Bv = 60 T) may smear this crossover.

Conclusions

Magnetoresistance in -YbAlB4 was measured in applied magnetic fields of up to 45 T. We detected a Fermi surface crossover with disappearance of the moderately large Fermi surface at 34 T in the intermediate valence state.

Acknowledgements

This work is partially supported by PRESTO, Japan Science and Technology Agency, Grants-in-Aid for Scientic Research (No. 25707030, 15J08663 and 25887015), by Grants-in-Aids for Scientic Research on Innovative Areas (15H05882, 15H05883) from Japanese Society for the Promotion of Science, Program for Advancing Strategic International Networks to Accelerate the Circulation of Talented Researchers (No.R2604) from the Japanese Society for the Promotion of Science and the Institute of Complex Adaptive Matter (ICAM). A portion of this work was performed at the National High Magnetic Field Laboratory, which is supported by National Science Foundation Cooperative Agreement No. DMR-1157490 and the State of Florida.

References

[1]	Y. Matsumoto., et al., Phys. Rev. B, 84, 125126 (2011).

[2]  E.C.T. O'Farrell et al., Phys. Rev. Lett, 109, 176405 (2012).

# Text boxes

Fig.1 Field dependence of the SdH oscillation osc above B = 25 T (1/B = 0.04 T-1). The lower panels shows FFT results for osc.