Enhancement of the Quadrupolar Quantum Critical Fluctuations by Pressure

Shimura, Y.; Nakatsuji, S.; Tsujimoto, M. (Institute for Solid State Physics, University of Tokyo); Zeng, B.; Zhang, Q. and Balicas, L. (NHMFL, FSU)

Introduction

The cubic PrV2Al20 with the 3 non-magnetic doublet ground state having orbital (quadrupole) degrees of freedom exhibits an antiferro-quadrupole ordering below 0.6 K. Recent pressure measurements for PrTi2Al20 the Ferro-quadrupole ordering found at ambient pressure below ~ 2 K becomes unstable and instead superconductivity with heavy quasi-particles at P ~ 8 GPa were observed below 1 K. Most likely, the superconducting pairing mechanism is associated with the quantum critical fluctuations of the quadrupole moments in the 3 non-magnetic doublet ground state. From the transport/bulk properties, including the quantum oscillation [1], PrV2Al20 is found located near the quadrupolar quantum critical point, when compared with PrTi2Al20. Indeed, PrV2Al20 is a heavy fermion superconductor and even undergoes field-induced quantum criticality at ~ 11 T for H // [111] at ambient pressure [2,3].

Experimental

We synthesized the single crystals for PrV2Al20 by an Al self-flux method, using a homemade vertical tube furnace. We measured magnetoresisitance  (H, T) for the magnetic field H // [111] under high pressure up to ~ 3 GPa by using piston cylinder type pressure cell at Cell 9 facility.

Results and Discussion

Figure 1 shows the field dependence of the resistivity at various pressures between 0 and 2.9 GPa at 0.36 K. We confirmed the main peak at 11 T, the critical field of the quadrupolar order phase with TQ = 0.6 K at close to the ambient pressure. With increasing pressure, the resistivity increases, especially near the critical field of 11 T as shown in Fig. 2 (upper). This suggests an enhancement of the quadrupolar fluctuations by pressure. Note that, as shown in Fig. 2 (lower), the full width at half maximum (FWHM) of the peak increases very rapidly above ~ 1.5 GPa by pressure. This suggests that the enhancement of the quadrupolar fluctuations smear out the boundary between the ordered state and para-quadrupole (no-ordered) state. This indicates that PrV2Al20 is approaching a quadrupolar quantum critical point by increasing the pressure.

Conclusions

We measured the magnetoresistance of single crystalline PrV2Al20 under pressures of up to ~ 3 GPa and high magnetic fields up to 31 T. The width of the peak at 11 T is divergently enhanced with pressure. This is probably due to the development of the quadrupole fluctuation.

Acknowledgements

This work is mainly supported by Grants-in-Aid for Scientific Research (No. 25707030, 15J08663 and 25887015), on Innovative Areas　(15H05882, 15H05883)　and Program for Advancing Strategic International Networks to Accelerate the Circulation of Talented Researchers (No.R2604) from the Japanese Society for the Promotion of Science.

References

[1] Y. Shimura et al., J. Phys.: Conf. Ser., 592 012026 (2015).

[2] Y. Shimura et al., Phys. Rev. B, 91, 241102(R) (2015).

[3] M. Tsujimoto et al., Phys. Rev. Lett., 91, 241102 (2014).

# Text boxes

Fig.2 The P-dep. of the resistivity value at peak position in (H) and zero field (upper panel) at 0.36 K. The lower panel shows a full width at half maximum (FWHM) of the peak 2 shown in Fig. 1

Fig.1 Field dependence of the resistivity (H) under various pressure up to 2.9 GPa at 0.36 K