Direct Band Gaps in Multiferroic h-LuFeO3

Musfeldt, J. L. ; Holinsworth, B.S.; Mazumdar, D. (Tennessee); Brooks, C.M.; Mundy, J.A.; Das, H.; Fennie, C.J.; Schlom, D.G. (Cornell); Cherian, J. and McGill, S.A. (NHMFL)

Introduction

The dream of room temperature ferroelectric ferromagnets is at the heart of the field of multiferroics and magnetoelectrics. Interface engineering is gaining traction in this regard. The idea is that by controlling composition and strain, room temperature exotic properties might emerge. One candidate for ferroelectric ferrimagnetism is a set of superlattices of the form (LuFeO3)n:(LuFe2O4)m.1 Here, n and m are layer indices that run from 0 to 4. The parent compounds, LuFe2O4 and LuFeO3, are well studied. LuFe2O4 is an antiferroelectric with a complex phase diagram, a series of charge ordering transitions above room temperature, and a 240 K ferrimagnetic ordering temperature. LuFeO3 is polar at 300 K and orders antiferromagnetically at 147 K in a pattern in which symmetry allows a slight canting of the spins giving rise to weak ferromagnetism. Preliminary findings of inter-grown layers suggests the tantalizing prospect of room temperature ferroelectric ferrimagnetism with ordering temperatures up to 280 K in certain members of the (LuFeO3)n:(LuFe2O4)m series.1 The need to understand the electronic structure of these engineered materials and complement susceptibility measurements with microscopic evidence for high temperature magnetism motivates our comprehensive optical absorption, magnetic circular dichroism, and photoconductivity measurements, and in order to place our superlattice work on a firm foundation, we begin with an investigation of pristine LuFeO3.

Results and Discussion

Figure 1 displays the crystal structure and character of the epitaxial thin films of LuFeO3 along with the optical absorption, magnetic circular dichroism, photoconductivity, and complementary first principles calculations.2 Our objectives were to (i) extract the band gaps, (ii) understand the excitations that form these gaps in terms of the partial densities of states, and (iii) test whether the films carry current in a device configuration. We also measured the dichroic response to correlate features in the dichroic rotation Δα(E) to the density of states and eventually to specific bands. This is useful and interesting because Δα(E) is directly proportional to magnetization. These experiments were carried out using the 25 T split-Florida helix. In the LuFeO3 end member, magnetic circular dichroism spectroscopy and analysis of the projected density of states provided incontrovertible evidence for a direct band gap at 1.1 eV involving minority channel excitations from hybridized Fe 3dz2 + O 2pz → Fe d at the Γ and A points, with a higher energy direct gap at 2.0 eV. Both charge gaps overlap nicely with the solar spectrum. This understanding of the LuFeO3 (and LuFe2O4) end members places experiments on the superlattices on a firm foundation. The development of a class of room temperature ferroelectric ferimagnets in thin film form will obviously promote many applications.

Fig. 1: (a, b) Crystal structure of LuFeO3 and transmission electron microscopy of an epitaxial thin film. (c,d,e) Optical absorption, magnetic circular dichroism, photoconductivity, and first principles calculations.2 This data resolved controversy about the electronic structure of LuFeO3 below 2 eV.

Acknowledgements

We thank the Materials Science Division, BES, U. S. DoE for support of this work (DE-FG02-01ER45885). A portion of this work was performed at the National High Magnetic Field Laboratory, which is supported by National Science Foundation Cooperative Agreement No. DMR-1157490 and the State of Florida.

References:

[1] P. Schiffer, unpublished results.

[2] Holinsworth, B. S. et al., Appl. Phys. Lett. 106, 182902 (2015).