Avalanches and Hysteresis at the Structural Transition in Stripe-Ordered La1.48Nd0.4Sr0.12CuO4

Baity, P.G.; Saraswat, G.; Popović, D. (Dept. of Phys. & Natl. High Magnetic Field Lab., FSU) and Sasagawa, T. (Tokyo Inst. of Tech.)

Introduction

The coupling or intertwining of lattice, spin and charge orders and their effects on superconductivity are of great current interest in the physics of cuprates.[1]  In particular, the low-temperature tetragonal (LTT) structure seems to stabilize static charge and spin stripes.  The rare-earth-doped cuprate La1.48Nd0.4Sr0.12CuO4 (LNSCO), for example, exhibits a first-order structural phase transition (SPT) from the low-temperature orthorhombic (LTO) to the LTT phase, with the onset of the charge stripe order roughly coinciding with the SPT. In general, the dynamics of first-order phase transitions in the presence of disorder have been well studied, although some questions remain open.  In the critical region, physical observables may exhibit hysteresis, return point memory, and a sequence of avalanches that link metastable states as the relevant field is tuned.[2,3] A previous study of the LTO-LTT transition in LNSCO by magnetoresistance (MR) measurements revealed hysteresis, which was attributed to a shift of the SPT temperature with an applied field.[4] However, the origin of the observed behavior was not well understood.

Experimental

Out-of-plane magnetoresistance has been measured on high quality LNSCO single crystals with x=0.12 near the LTO-LTT transition (TSPT =70.8±0.5 K) with H || c up to 12 T and H || ab up to 9 T. A standard four-probe dc reversal technique was used to measure resistance, and field sweep rates were low enough to avoid sample heating. Before each MR measurement, the sample system was prepared by warming to a high temperature  (usually ~90 K) to erase memory.

Results and Discussion

Hysteresis is observed for both field orientations, but for H || c we also find evidence for the existence of metastable states and collective dynamics in the form of avalanches and return point memory (Fig. 1). Such behavior indicates that, in LNSCO, the LTO-LTT structural transition can be driven with H.  A detailed analysis of the avalanche statistics is used to determine their size and field dependence, and to extract information about the domain structure and dynamics of domain walls.

Conclusions

Magnetoresistance measurements near the structural phase transition in LNSCO single crystals provide evidence for the presence of magneto-structural domains and their collective dynamics. These results shed light on the interplay of lattice, spin and charge degrees of freedom in stripe-ordered La-based cuprates.

Acknowledgements

This work was performed at the National High Magnetic Field Laboratory, which is supported by National Science Foundation Cooperative Agreement No. DMR-1157490 and the State of Florida. This work is also supported by NSF DMR-1307075.

References

[1] E. Fradkin et al., Rev. Mod. Phys, 87, 457 (2015).

[2] Eduard Vives et al., Phys. Rev. B 50, 3839 (1994).

[3] James P. Sethna et al., Phys. Rev. Lett. 70, 3347 (1993).

[4] Z. A. Xu et al., Europhys. Lett. 50, 796 (2000).

# Text boxes

Fig. 1 Out-of-plane MR measurent up to 9 T with H || c showing avalanches and return point memory near the LTO-LTT transition.