Superparamagnetism in the Martensitic Phase of Ni50-xCoxMn40Sn10

Yuan, S.; Hoch, M.J.R.; Kuhns, P.L.; Reyes, A.P. (National High Magnetic Field Laboratory, FSU);

Srivastava, V.; James, R.D. (U. Minnesota, Aerospace Engineering and Mechanics) and Leighton, C. (U. Minnesota, Chemical Engineering and Materials Science)

Introduction

The quaternary shape memory alloys Ni50-xCoxMn40Sn10 (5 ≤ x ≤ 8), exhibit low thermal hysteresis and a dramatic change in their magnetic properties across the martensitic transformation at temperatures TM > 300 K [1, 2]. These features are important for technological applications. The material transitions from ferromagnetic (F) in the austenite phase at T > TM to a weakly magnetic phase (no long-range order) in the martensitic phase at T <TM.

Experimental

Polycrystalline alloy samples (x = 0, 7 and 14) were produced by crushing melt-prepared ingots of high purity material. NMR spin echo measurements were made as a function of T in zero applied field by utilizing the very large internal hyperfine fields at 55Mn sites (20- 45 T).

Results and Discussion

The NMR spectra for x = 0, 7 and 14 samples at 1.6 K, given in Fig.1, show the emergence of new magnetic features with increasing x.  For x = 0 and 7 the spectra reveal mixed magnetic phases with coexisting F and antiferromagnetic (AF) clusters. Interestingly, for x = 7 there are two distinct F regions, attributed to high and low Co concentrations, respectively. The F clusters coexist with an inhomogeneous AF matrix at low T. Both F regions have nanoscale size distributions as derived from the spectral area vs.T plots over the range 1.6 – 200 K shown in Fig. 2. The distribution of F cluster radii (assuming spherical clusters) is shown as the inset in Fig. 2. The AF clusters are significantly smaller than the F and exhibit dynamical properties which make the signals unobservable for T > 10 K. The x = 14 alloy does not undergo a martensitic transition and has no AF component. This alloy again shows two F regions attributed to high and low local Co concentrations. For both x = 7 and 14 the results give a distribution of NMR blocking temperatures linked to distributions of nanocluster sizes. The variations in structure are likely due to the coexistence of mixed austenite and martensite nanophases.

Fig.1 55Mn NMR spectra for Ni50-xCoxMn40Sn10                                          Fig. 2  55Mn NMR spectral areas for Ni43Co7Mn40Sn10

(x = 0, 7 and 14) at 1.6 K:  AF (blue) and F (red)                          vs. T:  AF (blue) and F (red)

Conclusions

Hyperfine field NMR provides a powerful means for obtaining information on the magnetic nature of the Ni-Co-Mn-Sn alloys at the nanoscale. The findings provide considerable insight into the origins of the macroscopic magnetic behavior of these materials.

Acknowledgements

A portion of this work was performed at the National High Magnetic Field Laboratory which  supported by National Science Foundation Cooperative Agreement No. DMR-1157490 and the State of Florida. Work by CL’s group at UMN supported by DOE under DE-FG02-06ER46275 and by RDJ’s group under AFOSR-MURI, NSF-PIRE(OISE-09671) and ONR (N00014-14-1-0714).

References

[1]	Bhatti, K.P., et al., Phys. Rev. B 85, 134450 (2012).

[2]  Bhatti, K.P., et al., in Heusler Alloys, edited by A. Hirohata and C. Felser (Springer, 2015).