Specific Heat and Magnetization of Ba3Co2O6(CO3)0.7

Padgett, A.S.; Takano, Y. (UF, Physics); Lee, M.; Choi, E.S. (NHMFL); Sakakibara, T. (ISSP, U. Tokyo); Dun, Z.L. and Zhou, H.D. (U. Tennessee, Physics)

Introduction

Ba3Co2O6(CO3)0.7, a compound related to perovskites, is a new candidate for a quantum spin liquid [1]. 135Ba NMR in this material exhibits no change in linewidth down to 0.48 K, with a temperature-independent tau2, indicating that the Co spins are magnetically disordered. The specific heat shows no sign of ordering down to 2 K and contains a term linear in temperature, suggestive of a gapless spin-liquid ground state.

Experimental

Single crystals of Ba3Co2O6(CO3)0.7 were grown by a flux method [1,2]. Using relaxation calorimetry, vibrating-sample magnetometry (VSM), and force magnetometry, we have measured the specific heat and magnetization of this compound at the NHMFL DC-Field Facility.

Results and Discussion

Figure 1 shows the specific heat divided by temperature as a function of temperature between 0.17 K and 2.3 K. For measurements in magnetic fields, the field was applied along the crystallographic c axis. The data exhibit unambiguous linear behavior at low temperatures, as well as 1/T2 behavior attributable to a nuclear Schottky contribution. The linear term depends only weakly on the magnetic field, at least up to 9 T.

Magnetization results are shown in Fig. 2. The data up to 35 T were taken at 1 K by using a VSM; those up to 18 T were taken at 18 mK with force magnetometry. The magnetization is highly anisotropic, as has been reported [1], and does not saturate even at 35 T. With the c axis parallel to the magnetic field, the magnetization is a non-linear function of magnetic field. At present, the mechanism behind the strong nonlinearity of the magnetization curve is not understood.

For systems exhibiting T-linear behavior in specific heat, be they conduction electrons or gapless spin liquid, the Wilson ratio, RW, is a useful parameter that assists in identifying the ground state and the nature of low-lying gapless excitations. We find RW = 36.9±0.7 at zero field and 29.7±0.8 at 9 T. These are unusually large values. We plan to extend our measurements to higher magnetic fields.

Acknowledgements

This work was supported by the National Science Foundation (NSF) under Grant No. DMR-1350002. A portion of the work was performed at the National High Magnetic Field Laboratory, which is supported by NSF Cooperative Agreement No. DMR-1157490, the State of Florida, and the U.S. Department of Energy.

# Text boxes

Fig.1 Specific heat of Ba3Co2O6(CO3)0.7.

References

[1]	Igarashi, H., et al., Phys. Rev. B 89, 054431 (2014).

[2]	Iwasaki, K., et al., J. Appl. Phys. 106, 034905 (2009).

Fig.2 Magnetization of Ba3Co2O6(CO3)0.7 at 1 K and 18 mK.