Phase Diagram of the Quasi-Two-Dimensional Antiferromagnet USb2

Via Fiber Bragg Dilatometry in Pulsed Magnetic Fields

Stillwell, R.L.; Jeffries, J.R. (Lawrence Livermore National Laboratory); Jaime, M. (NHMFL-PFF); Butch, N.P. (National Institute of Standards and Technology and U. Maryland); Liu, I.-L. (National Institute of Standards and Technology and U. Maryland)

Introduction

The uranium dipnictides, UX2 (X= P, As, Sb, Bi), show unusual transport and magnetization properties due to their highly anisotropic, quasi-two-dimensional nature[1, 2]. These materials consist of antiferromagnetically ordered uranium layers aligned along the c-axis in either an up-down or up-down-down-up configuration [3].  It has also been shown that the 5f-electrons from the uranium ions are hybridized with the conduction electrons[4].

Experimental

USb2 single crystals were grown via a self-flux technique with excess Sb, using a U:Sb ratio of 1:6. Magnetostriction and thermal expansion measurements were performed via an optical fiber Bragg grating (FBG) dilatometer [5, 6] in pulsed magnetic fields up to 65 T at the National High Magnetic Field Pulsed Field Facility at Los Alamos National Laboratory.

Results and Discussion

Our results revealed the antiferromagnetic to paramagnetic phase transition in USb2 via a fiber Bragg grating dilatometer (Fig. 1) in which we were able to follow the transition from T=203-80K using pulsed magnetic fields up to 65T.  The observed transition sharpens significantly below T= 150K, with the strain as a function of magnetic field going from H2-like for fields below the transition to independent of H above the transition.

Conclusions

We believe that this behavior suggests a possible AFM to spin-flop transition for T< 150 K, similar to the classical antiferromagnet MnF2 [7]. Future experiments need to be performed using high-magnetic field magnetization techniques to study the magnetic structure above the field-induced suppression of the AFM phase.

Acknowledgements

A portion of this work was performed at the National High Magnetic Field Laboratory, which is supported by National Science Foundation Cooperative Agreement No. DMR-1157490, the State of Florida and the U.S. Department of Energy.  This work was also performed under LDRD (Tracking Code 14-ERD-041) and under the auspices of the US Department of Energy by Lawrence Livermore National Laboratory (LLNL) under Contract No. DE-AC52-07NA27344.

References

[1] R. Wawryk, Philos. Mag., 86, 1775-1787 (2006).

[2] D. Aoki, et al., Philos. Mag. B, 80, 1517-1544 (2000).

[3] J. Leciejewicz, et al., Physica Status Solidi (B), 22, 517-526 (1967).

[4] E. Guziewicz, et al., PRB, 69, 045102, (2004).

[5] R. Daou, et al., RSI, 81, 5 (2010).

[6] M. Jaime, et al., PNAS, 109, 12404-12407 (2012).

[7] Y. Shapira, et al., PRB, 1, 3083-3096 (1970).

# Text boxes

Fig. 1 Strain versus applied magnetic field of USb2 at various temperatures below the AFM transition. The AFM transition is marked with a dashed line for clarity and the traces are vertically offset for ease of viewing the transition. The sharpening of the transition as the temperature is lowered suggests a possible crossover from AFM-PM for T>140K, to AFM-spin-flop transition for T<140K.