Strong Magnetoelectric Coupling in Ti Doped Ca3Ru2O7 Single Crystal in Pulsed Magnetic Fields

Lei, S.; Akamatsu, H.; Gopalan, V. (Penn State); Chikara, S.; Singleton, J.; Zapf, V. (LANL); Rondinelli, J.M. (Northwestern); Mao, Z.Q. (Tulane) and Ke, X. (Michigan State)

Introduction

Ca3Ru2O7 is known to undergo a paramagnetic (PM)-antiferromagnetic (AFM) transition at TN=56 K [1], followed by a first-order metal-insulator transition (MIT) at TMIT =48 K, with a reentrance to metallic state below T=30 K [2]. Our recent density functional calculations (DFT) have shown that Ti doped Ca3Ru2O7 has a canted antiferromagnetic ground state, with a potentially strong magnetoelectric coupling. Therefore it is essential to establish the magnetic properties in this system.

Experimental

The change in magnetization (M) was measured on Ti-doped single crystal Ca3Ru2O7 as a function of magnetic field μ0H up to 65 Tesla in short-pulse magnets at the NHMFL-PFF. M was measured by integrating the voltage induced in a triply-compensated coil during sample in and sample out shots [3,4].

Results and Discussion

Shown below are our summarized results based on the M measurement for magnetic field H|| a-axis in the crystal.

Conclusions

Our current results are only based on field H|| a-axis only. From figure (b), signatures of three phase transitions under ramping magnetic field at low temperature were observed. The high field (~22 T) and low field (~5 T) peaks are signatures of first order transitions with hysteresis. The transition at ~13 T has no hysteresis. We are planning the measurements on other two orthogonal directions to complete our phase diagram mapping.

Acknowledgements

We acknowledge primary support from the National Science Foundation grant number DMR-1210588. The National High Magnetic Field Laboratory facility is supported by National Science Foundation Cooperative Agreement No. DMR-1157490, the State of Florida, and the U.S. Department of Energy.

References

[1] Cao et al. Phys. Rev. Lett. 78, 1751 (1997).

[2] Yoshida et al. Phys. Rev. B 69, 220411(R) (2004)

[3] Goddard et al, New J. Phys. 10, 083025 (2008)

[4] V. S. Zapf et al, Phys. Rev. B 82, 060402 (2010)

# Text boxes

(a)

(b)

(a) M(H) measured under pulsed magnetic field (b) Phase diagram built from the peak positions of  the first derivative of M(H) curve in the figure (a)