Infrared Magneto-Spectroscopy Study of Phase Transition

in InAs/GaSb Quantum Well Bilayers

Jiang, Y.; Jiang Z. (Georgia Tech); Ludwig, J.; Smirnov, D. (NHMFL); Saha, D.; Stanton, C.J. (Univ. of Florida); Hawkins, S.D.; Klem, J.F. and Pan, W. (Sandia National Labs)

Introduction

InAs/GaSb quantum well bilayer system has recently aroused much interest, because it can host novel quantum phases [1] with different band alignment [Fig 1(a)] via changing the relative thickness between two quantum wells [Fig 1(b)]. It has been found that the conduction band of InAs can be tuned from above to below the valence band of GaSb, through a gapless state [Fig 1(b)] where the conduction band meets the valence band at the center of the Brillouin zone. Such tunability promotes InAs/GaSb quantum well bilayer as an important playground for exploring fundamental phenomena such as excitonic insulator and quantum spin Hall effect.

Experimental

To change the relative thickness between the two quantum wells, we fix GaSb to 5 nm and vary the thickness of InAs from 8, 10, 11, 13, to 15 nm. Magneto-transmission spectra through these samples were measured in SCM-3 with a Fourier transform infrared spectrometer in magnetic fields up to 17.5 T.

Results and Discussion

In the normal and critical regions, only one cyclotron resonance (CR) was observed [Fig. 1(c)]. As the system moves into an inverted state, multiple CRs as well as anti-crossing behavior start to emerge [Fig. 1(d)]. Our observation can be attributed to the mixing of the electron and hole Landau levels, which is greatly enhanced in the inverted region. In addition, in the 15nm sample, we observed a hole-like transition at high magnetic fields, indicative of a heavily inverted band structure.

Conclusions

By studying the infrared magneto-transmission of InAs/GaSb quantum well bilayers from the normal to inverted region, we observed multiple CRs developed as the system moves across the critical region where a quantum phase transition occurs. The lack of Landau level mixing in the sample at the critical thickness may be suggestive of the opening of an excitonic gap.

Acknowledgements

The infrared measurement was supported by the Department of Energy (Grant No. DE-FG02-07ER46451), and performed at the National High Magnetic Field Laboratory, which is supported by National Science Foundation Cooperative Agreement No. DMR-1157490 and the State of Florida. Z.J. acknowledges the support from the NHMFL Visiting Scientist Program. Work at Sandia was supported by the Department of Energy, Office of Science, Basic Energy Sciences, Materials Sciences and Engineering Division. Sandia National Laboratories is a multi-program laboratory managed and operated by Sandia Corporation, a wholly owned subsidiary of Lockheed Martin Corporation, for the U.S. Department of Energy’s National Nuclear Security Administration under contract DE-AC04-94AL85000.

References

[1] Pezzini S. et al. submitted (2015).

# Text boxes

Fig.1: (a) Band diagram and thickness of each quantum well material. The H0 and E0 represent hole and electron subbands in different quantum wells, respectively. (b) Evolution of the conduction (red) and valence (black) band alignment from normal to inverted region with increasing thickness x of the InAs quantum well. (c,d) Normalized transmission spectra in normal/critical (c) and inverted (d) regions at selected magnetic fields.