Current Density in Superconducting CORC® Cables Exceeding 300 A/mm2 at 20 T

van der Laan, D.C. (Advanced Conductor Technologies and the University of Colorado); Weiss, J.D. (University of Colorado); Noyes, P. and Godeke, A. (FSU-NHMFL)

Introduction

The next generation of high-field magnets requires operating fields exceeding 20 T and that cannot be reached with low-temperature superconductors, such as NbTi or Nb3Sn and high-temperature superconductors (HTS), such as REBa2Cu3O7- (REBCO) coated conductors, are the only option. The measurements performed at the user facility of the NHMFL are in support of Conductor on Round Core (CORC®) cable development [1-2]. This year we’ve reached a new record engineering current density Je of 309 A/mm2 at 4.2 K and 20 T (projected), making CORC® cables the most promising HTS cables for high-field magnets.

Experimental

A 5.1 mm diameter CORC® cable was wound from 50 superconducting tapes. The tapes were purchased from SuperPower and contained extra thin substrates of 30 m thickness to help increase the cable current density. The thinner substrate allowed us to wind the tapes on a former of only 3.2 mm in diameter, resulting in a performance retention of 97 % before testing at high field.

a. b.

Figure 1. a) Voltage vs. current at 4.2 K the CORC® cable at 17 T. b) Field dependence of the critical current at 4.2 K.

Results and Discussion

The CORC® cable had a critical current Ic of 7,030 A in a field of 17 T. The superconducting transition is shown in Fig. 1a, together with a fit to determine Ic. The current density of the 5.1 mm diameter CORC cable at 17 T was 341 A/mm2. Based on the field dependence of Ic of CORC® cables as shown in Fig. 1b, Je at 20 T is expected to be a record 309 A/mm2, almost 50 % higher than the old record of 216 A/mm2 reached in 2014.

Conclusions

The results obtained at the user facility of the NHMFL in 2015 clearly show the potential of CORC® cables for use in high-field magnets. The record engineering current density at 20 T of 309 A/mm2 is as far as we know the highest current density measured in any HTS cable at that field. The results confirm that CORC® cables are suitable for use in magnets ranging from large fusion magnets operating at high currents to accelerator magnets operating at very high current densities.

Acknowledgements

This work was supported in part by the U.S. Department of Energy, under award numbers DE-SC-0007891, DE-SC0009545, and DE-SC0014009. A portion of this work was performed at the National High Magnetic Field Laboratory, which is supported by National Science Foundation Cooperative Agreement No. DMR-1157490, the State of Florida, and the U.S. Department of Energy.

References

[1] 	van der Laan, D.C., et al., Supercond. Sci. Technol. 26, 045005 (2013).

[2] 	van der Laan, D.C., et al., Supercond. Sci. Technol. 28, 124001 (2015).