Ic Study of Thick MOCVD REBCO Coated Conductors for

High Field Magnet Applications

Xu, A. (UH, TcSUH); Jaroszynski, J.; Abraimov, D.; Larbalestier, D.C. (FSU, NHMFL) and Selvamanickam, V. (UH, Mechanical Engineering)

Introduction

Our previous work at the NHMFL has demonstrated that Zr incorporation can significantly increase critical current density Jc and substantially reduce Jc anisotropy of REBCO coated conductors which is highly beneficial for very high field magnet applications.  Growing thicker REBCO layer is a more direct strategy to reach higher critical current Ic. However, thickness increment has long been obstructed due to microstructure degradation with increasing REBCO layer thickness. Recently, by modifying the MOCVD process, we have successfully grown (3 (m thick, 20% Zr-added REBCO coated conductor with much reduced microstructure degradation.

Experimental

High density of BZO nanorods was self-assembled in the epitaxial REBCO films by 20 mol.% Zr-doping. (3.0 (m thick REBCO layer was grown using a three-pass MOCVD process. Ic(H||c) characterization was conducted at 4 K and magnetic fields up to 31 T at the NHMFL.

Results and Discussion

As shown in the insets of Fig. 1, the microstructure degradation, including high density a-axis grains, big second phase particles, and degraded BZO nanorod growth is present in a previously-made (3 (m thick 15% Zr-added coated conductor. Such microstructure degradation is significantly reduced in the recent ~3 µm thick 20% Zr-added tape, leading to more than 60% higher Je and Ic enhancement, where Je, an important parameter for magnet design, is defined by dividing Ic by the whole cross section of REBCO tape.

Conclusions

We attribute this excellent Ic partially to the thicker REBCO layer and partially to the pinning enhancement owing to the higher Zr-addition.

Acknowledgements

A portion of this work was performed at the National High Magnetic Field Laboratory, which is supported by National Science Foundation Cooperative Agreement No. DMR-1157490 and the State of Florida. The work at the University of Houston was partially funded by Advanced Research Projects Agency-Energy (ARPA-E) award DE-AR0000196 and Argonne National Laboratory award 4F-30201.

References

[1] Selvamanickam, V., et al., Appl. Phys. Lett. 106, 032601 (2015)

[3] Selvamanickam, V., et al., Supercond. Sci. Technol. 28, 072002 (2015)

# Text boxes

Fig. 1 Je(H||c) (left vertical axis) and the corresponding Ic(H||c) for 4 mm wide tape (right vertical axis) for (a) an early (3 (m thick, 15% Zr + REBCO coated conductor, and (b) a (3 (m thick, 20% Zr + REBCO coated conductor.  The TEM images in the insets show substantially reduced microstructure degradation in the (3 (m thick, 20% Zr-added sample.