Persistent Superconducting Joint between Bi-2212/Ag-alloy

Multifilamentary Round Wires

Chen, P.; Trociewitz, U.P.; Davis, D.; Abraimov, D.; Starch, W.; Hilton, D.; Kim, Y.; Bosque, E.; Jiang, J.; Hellstrom, E.E. and Larbalestier, D.C. (ASC, NHMFL)

Introduction

Superconducting joints are one of the key components needed to make Ag-alloy clad Bi2Sr2CaCu2O8+x (Bi-2212/Ag) superconducting round wire (RW) successful for high-field, high-homogeneity magnet applications, especially for nuclear magnetic resonance (NMR) magnets in which persistent current mode (PCM) operation is usual in Nb-based magnets. A procedure for fabricating a superconducting joint between Bi-2212/Ag RWs was successfully developed and tested [1, 2].

Experimental

The voltage-current (V-I) properties of joints were evaluated using a standard four-point method at 4.2 K and background magnetic fields from 0 T to 14 T. The joint microstructures were examined by scanning electron microscopy (SEM).

Results and Discussion

Figure 1(a) shows the V-I properties of a typical Bi-2212 superconducting joint at 4.2 K and multiple magnetic fields up to 14 T. AIt is clear that a maximum supercurrent of ~ 850 A was achieved at self-field. With increase of external field, the supercurrent was gradually suppressed as expected, ~ 450 A supercurrent was achieved at 14 T. Figure 1(b) shows the longitudinal cross-sectional image of a typical Bi-2212 superconducting joint. The microstructure clearly shows that the interface of Bi-2212/Ag RWs is enclosed with well textured Bi-2212 crystal colonies, resulting in a well-connected superconducting network between Bi-2212 filaments.

| (a). | (b). |
| --- | --- |

Figure 1. (a). V-I properties of a typical joint at 4.2 K; (b). SEM images of longitudinal cross-section of a typical joint.

Conclusions

We successfully developed a fabrication procedure for a superconducting joint between Bi-2212/Ag RWs for persistent current operation. The V-I properties of a typical Bi-2212 superconducting joint were characterized at 4.2 K and multiple magnetic fields up to 14 T. The microstructure of a typical Bi-2212 superconducting joint was also evaluated using SEM, which clearly shows the continuous Bi-2212 path.

Acknowledgements

This work was supported by the National Science Foundation DMR-1157490 and by the State of Florida. We thank Dr. Seungyong Hahn for valuable discussions. Technical support from Lamar English and George Miller is also greatly acknowledged.

References

[1] Trociewitz, U.P., et al., “A Practical Superconducting Electrical Joint Design for High Temperature Superconducting Bi2Sr2CaCu2O8+x (B-2212) Round Wire” (US patent pending, 62129266, March-2015).

[1] Chen, P., et al., “Development of a Superconducting Joint between Bi-2212/Ag-alloy Multifilamentary Round Wires for Persistent Current Mode Operation” (in preparation for publication).