Seebeck Coefficient of Underdoped La2−xSrxCuO4 in High Magnetic Fields:

Fermi-Surface Reconstruction by Charge-Density-Wave Order

Badoux, S.; Afshar, S.A.A.; Michon, B.; Ouellet, A.; Fortier, S.; Doiron-Leyraud, N.; Taillefer, L. (U. de Sherbrooke); LeBoeuf, D. (LNCMI Grenoble); Croft, T.P.; Lester, C.; Hayden, S.M. (U. of Bristol); Takagi, H. (U. of Tokyo); Yamada, K. (IMSS Tsukuba) and Graf, D. (NHMFL)

Introduction

The recent observation of charge-density wave (CDW) order in underdoped YBa2Cu3Oy [1] was a pivotal development that opened up a new era of research on high-temperature cuprate superconductors. Now observed in essentially all cuprates, CDW order appears to be one of their universal properties. But in some cuprates, the CDW is also accompanied by spin-density-wave (SDW) modulations, which naturally begs the following question: is CDW order intertwined with SDW order, as in the well known “stripe state”, or is it independent?

Experimental

We examined this question via a series of high-magnetic field transport experiments at the NHMFL on the classic cuprate material La2-xSrxCuO4 (LSCO). Our high-field thermopower measurements reveal a clear signature of the CDW in LSCO, as a negative Seebeck coefficient at low temperature [2] (see Fig. 1a), just as found in our prior work on YBCO [3], Hg1201 [4], and Eu-LSCO [5]. Using this signature we closely tracked the CDW as a function of doping across the phase diagram of LSCO and reached the following conclusion: in the field-induced normal state of LSCO, the CDW phase terminates at the critical doping pCDW = 0.15 [2], as shown in Fig. 1b.

Results and Discussion

LSCO is of particular interest since it exhibits both SDW order and CDW modulations [6]. Furthermore, in LSCO the SDW order as observed by neutron scattering measurements is enhanced by a magnetic field [7] and terminates, in the absence of superconductivity, at a doping of approximately pSDW ~ 0.2. Prior electrical resistivity experiments have also revealed a quantum critical point at pSDW ~ 0.2 [8], consistent with it being the termination of the SDW phase. This is distinctly above the critical point for CDW at pCDW = 0.15 revealed by our work [2].

Conclusions

This clear separation of pCDW and pSDW is strong evidence that CDW and SDW in cuprates are separate phenomena, contrary to the long-held notion that CDW and SDW modulations are fundamentally intertwined in a single state of “stripe order”. It also sheds new light on the origin of the quantum critical linear-T resistivity in LSCO [8].

Acknowledgements

A portion of this work was performed at the NHMFL, which is supported by National Science Foundation Cooperative Agreement No. DMR-1157490 and the State of Florida. A portion of this work was performed at the LNCMI of France. We acknowledge support from CIFAR, NSERC, FRQNT, CFI, and a Canada Research Chair.

References

[1]	Wu, T., et al., Nature 477, 191 (2011); Ghiringhelli, G. et al., Science 337, 821 (2012).

[2]	Badoux, S., et al., arXiv:1512.00292.

[3]	Chang, J., et al., Phys. Rev. Lett. 104, 057005 (2010).

[4]	Doiron-Leyraud, N., et al., Phys. Rev. X 3, 021019 (2013).

[5]	Laliberté, F., et al., Nat. Commun. 2, 432 (2011).

[6]	Croft, T., et al., Phys. Rev. B 89, 224513 (2014).

[7]	Chang, J., et al., Phys. Rev. B 78, 104525 (2008).

[8]	Cooper, R. A., et al., Science 323, 603 (2009).

# Text boxes

Fig. 1: a) Seebeck coefficient S of LSCO with doping x = 0.07 and 0.125, plotted as S/T vs temperature T, in magnetic fields as shown. The drop in S/T at Tmax for x = 0.125 is caused by Fermi surface reconstruction, a signature of the CDW [2]. b) Temperature-doping phase diagram of LSCO, showing the onset temperature for CDW (TCDW) measured by       X-rays [6]. Our work shows that Tmax = 0 at pCDW = 0.15, where the CDW order ends [2].