Upper Critical Field for the High-Tc Cuprate HgBa2CuO4+δ

Chan, M.K.; McDonald, R.D.; Harrison, N. (NHMFL, Los Alamos) and Greven, M. (University of Minnesota)

Introduction

A measurement of the upper critical field with doping in the cuprates is expected to provide valuable insight into the evolution of the strength of superconductivity within the phase diagram1. It can thus serve to provide insight into the relationship between superconductivity and other competing phases. The proposed experiment is to measure the upper critical field in the single layer cuprate HgBa2CuO4+δ (Hg1201).

Experimental

Experiments were performed with the 65T short pulse magnet at various temperatures utilizing resistivity measurements.

Results and Discussion

We have successfully measured Hc2 at a number of doping levels. These measurements allow us to determine that phases such as charge and spin-density waves and q=0 magnetism do indeed impact the strength of superconductivity.

Acknowledgements

This work, performed at Los Alamos National Lab, was supported by the US Department of Energy BES

“Science at 100 T" grant no. LANLF100. The National High Magnetic Field Laboratory facility is supported by National Science Foundation Cooperative Agreement No. DMR-1157490, the DOE, and the State of Florida. Work at the University of Minnesota was supported by the Department of Energy, Office of Basic Energy Sciences, under Award No. DE-SC0006858.

References

[1]	Grissonnanche, G. et al. Direct measurement of the upper critical field in cuprate superconductors. Nat. Commun. 5, 3280 (2014).