Atomic Resolution Imaging of Heterostructure Interfaces of 2D Transition Metal

Dichalcogenide Monolayer

Xin, Y. (NHFML), Sahoo, P.K. (USF, Physics), Memaran, S. (FSU, Physics), Balicas, L. (FSU, Physics, and NHMFL) and Gutiérrez, H.R. (USF, Physics)

Introduction

Transition metal dichalcogenide (TMD) monolayers are atomically thin semiconductors of the type MX2, with M a transition metal atom (Mo, W, etc.) and X a chalcogen atom (S, Se, or Te). TMD monolayers MoS2, WS2, MoSe2, WSe2, have a direct bandgap, and can be used in electronics as transistors and in optics as emitters and detectors. The work on TMD monolayers is an emerging research field since the discovery of the direct bandgap and two-dimensional heterojunctions have great potential for application in low power, high-performance and flexible electro-optical devices. In our work, we developed a method of one-pot growth of sequential edge-epitaxial heterostructures with WSe2/MoSe2 or WS2/MoS2. We are able to grow multi-junction heterostructures by selective water-oxidation and volatilization [1].

Experimental

High-angle-annular-dark-field-scanning transmission electron microscopy (HAADF-STEM) is used to image the WSe2/MoSe2 heterostructure interfaces. An aberration-corrected JEM-ARM200cF was used to image the monolayers of MoSe2 and WSe2. The images were acquired with a probe size 7c, 8cm camera length, which has a STEM resolution of 0.78 Å and inner collection angle of 76 mrad. The atom intensity is proportion to Z1.7, so the W atom shows brightest contrast, Mo has less intensity, and the Se is the weakest ones.

Results and Discussion

Fig.1a is the photoluminescence intensity maps of a triangle-shaped single crystal that has a multilayer heterostructures [1]. The low magnification image shows two interfaces 1 and 2 that follows the growth sequence (Fig.1b). The atomic resolution image shows one W atom with two Se atoms in WSe2 (Fig.1c), and one Mo atom with two Se atoms (Fig.1d). The interface images (Fig.1e-1f) clearly shows that the MoSe2 grows after WSe2 has sharp interface, but the interface has a transition width following growth from MoSe2 to WSe2.

Acknowledgements

TEM work was performed at the National High Magnetic Field Laboratory, which is supported by National Science Foundation Cooperative Agreement No. DMR-1157490 and the State of Florida. This work was supported by the National Science Foundation (NSF) grant DMR-1557434 and the US Army Research Office MURI grant W911NF-11-1-0362 and the Office Naval Research DURIP Grant 11997003.

References

[1]	Sahoo, P. K. et al., Nature, to be published, Jan. 4, (2018).

Fig.1 Photoluminescence intensity maps and HAADF-STEM images of the WSe2/MoSe2 heterostructures.