Quantum Hall and Magneto-Photoluminescence Measurements in WSe2

Jauregui, L.A., Joe, A.Y., Pistunova, K. (Harvard, Physics); Lu, Z. (FSU, Physics, NHMFL); Smirnov, D. (NHMFL); Kim, P. (Harvard, Physics)

Introduction

Single layer, 2-dimensional (2D) transition metal dichalcogenides (TMDs), such as WSe2, are direct bandgap atomically thin semiconductors that provide a unique platform for novel optoelectronic devices and device physics. Due to broken inversion symmetry in the single-layer limit, TMDs have spin-valley locking physics that can be explored for and utilized in such devices. Using a stamp-on-contacts method, we fabricate high quality, dual-gated WSe2 devices passivated with boron nitride (BN) (Fig.1a-b). The fabricated devices have transparent contacts down to cryogenic temperatures that allow for observation of Shubnikov de Haas (SdH) oscillations and the quantum Hall effect. When electrostatically doped WSe2 is optically excited at low temperatures, photoluminescence (PL) spectra show both exciton and trion species. In a perpendicular magnetic field, the g-factors of the exciton and trion peaks can be extracted from the Zeeman splitting.

Experimental

Quantum hall measurements were performed with magnetic fields up to 31 T in Cell 9 at DC Facility. Magneto-PL measurements were performed with magnetic fields up to 14 T with the 15/17 T magnet at the EMR Facility.

Results and Discussion

Fig.1 (a) Cartoon of WSe2 device with platinum contacts, encapsulated by BN layers. (b) Optical image of a characteristic device. (c) SdH at T = 300 mK and at n = 1.1X1012 cm-2 shows integer filling factors, indicating the lifting of degeneracy. All integer filling factors from ν = 7 down to ν = 2 are indicated. Inset: band diagram of WSe2 for low doping when the Fermi level is above one of the spin split valence bands. (d) Magnetic field dependence of PL under excitation by unpolarized 660nm laser at VBG= -18V. Splitting of charged exciton (X-) and defect peak (L1) is observed at high B with a trion g-factor ~11. X0 indicates the neutral exciton. (e) VBG dependence of PL at B = 14T shows X- splitting and varies with applied VBG.

Acknowledgements

A portion of this work was performed at the National High Magnetic Field Laboratory, which is supported by National Science Foundation Cooperative Agreement No. DMR-1157490 and the State of Florida. The experimental work at the magnet lab is supported by DOE (DE-SC0012260). Device fabrication and optical characterization is supported by AFOSR MURI (FA9550-17-1-0002). P.K. acknowledges partial support from the Gordon and Betty Moore Foundation's EPiQS Initiative through Grant GBMF4543.

References

[1]	Fallahazad, B., et al., Phys. Rev. Lett., 116, 086601 (2016).

[2]	Movva, H.C.P., et al., ACS Nano, 9 (10), 10402-10410 (2015).