Magneto-Photoluminescence Spectroscopy of Interlayer Exciton in

van der Waals Heterostructures

Wang, T., Li, Z. (Rensselaer Polytechnic Institute (RPI), Chemical Engineering); Lu, Z. (NHMFL, FSU Physics); Meng, Y., Chen, Y. (RPI Chemical Engineering); Smirnov, D. (NHMFL); Shi, S. (RPI, Chemical Engineering)

Introduction

Transition metal dichalcogenides (TMDCs) represent a new class of atomically thin semiconductors with superior optical and electrical properties. A Van der Waals heterostructure of TMDCs provides a method to construct atomically sharp interface with atomic level control and provides a unique playground for low dimensional physics. In particular, a type II alignment can be formed by a single layer MoSe2/WSe2 resulting in a large band offset and long-lived interlayer excitons [1]. Magneto-photoluminescence spectroscopy of the interlayer exciton will not only shed light on its origins but also provides guidance for future valleytronics applications.

Experimental

Single layer MoSe2 and WSe2 were exfoliated and then transferred to the SiO2/Si substrate. A thin layer of hexagonal boron nitride (h-BN) was transferred on top of the heterostructure to ensure minimum exposure to air. Contacts were fabricated by e-beam lithography followed by gold evaporation. The magneto-PL measurements were performed using a direct-optics micro-spectroscopy setup coupled to the 15/17 T SC magnet (EMR facility).

Results and Discussion

The low temperature photoluminescence (PL) spectra show the interlayer exciton at ~ 1.35 eV, similar to the previous report [1]. The left-circular polarized excitation (K) favorably generates left-circular polarized emission (K) rather than right-circular polarized light (K’). The valley polarization is about 30% and is smaller than that from intralayer exciton, which is about 70%. The external magnetic field up to 14.5 T does not generate obvious Zeeman splitting of the interlayer exciton peak, indicating small g factor. Meanwhile, we also note that the rich spectra feature from the defects close to intralayer exciton peaks is worth investigating.

Fig.1 (a) Microscope image of the MoSe2/WSe2 heterostructure encapsulated by h-BN.  Scale bar: 10 µm. (b, c) PL spectra measured with different chiral excitations at 0 T (b) and 14.5 T (c).

Conclusions

We have successfully shown the presence of the valley polarized interlayer exciton and have studied the B field dependence of the PL. Surprisingly, the Zeeman splitting of the interlayer exciton is small. The exact mechanism is still under investigation.

Acknowledgements

A portion of this work was performed at the National High Magnetic Field Laboratory, which is supported by National Science Foundation Cooperative Agreement No. DMR-1157490 and the State of Florida. S. Shi acknowledges the startup fund from RPI.

References

[1] Rivera, P., et al., Science, 351, 688 (2016).