Tuning Ising Superconductivity with Layer and Spin-Orbit Coupling

in Two-Dimensional Transition Metal Dichalcogenides

de la Barrera, S.C., Sinko, M.R., Gopalan, D.G. (Carnegie Mellon, Physics); Tsen, A.W. (Waterloo, Physics); Xu, X. (U. Washington, Physics); Xiao, D. and Hunt, M.B. (Carnegie Mellon, Physics)

Introduction

Superconductivity in the presence of strong spin-orbit coupling (SOC) is predicted to lead to novel electronic phases in two dimensions. The addition of broken inversion symmetry is expected to enforce a significant portion of spin-triplet Cooper pairs. Experimental progress in isolating and protecting atomically-thin, superconducting transition metal dichalcogenide (TMD) crystals has enabled investigations of these intriguing phenomena in the two-dimensional limit. In particular, a novel superconducting phase resulting from strong SOC and broken inversion symmetry known as “Ising superconductivity” has been measured in monolayer (1L) TaS2 [1] and NbSe2 [2], revealed by low-temperature and high-field measurements of the parallel upper critical field, Hc2||, which is significantly enhanced over the paramagnetic limit. These measurements have raised several important questions about the precise nature of this state, such as the importance of the triplet fraction of pairing, the origin of the upper critical field, and the possibility of supporting unconventional and/or topological superconducting phases.

Experimental

We performed magnetotransport measurements on single- and few-layer TaSs and NbSe2 devices in both Cell 9 and Cell 12 as a function of the temperature and the magnetic field, taking great care to ensure the precise parallel orientation of the two-dimensional plane of the superconductors with respect to the field.

Results and Discussion

Figure 1 shows our results for the upper critical field of atomically-thin TaS2 and NbSe2 in parallel fields, extracted from temperature- and field-dependent measurements of the resistance. The upper critical fields are significantly larger than the predicted paramagnetic limit, Hc2||/HP »1, for all devices measured. Comparing 1L TaS2 and NbSe2, we find that the enhancement above HP is larger for TaS2 than NbSe2 due to the larger SOC in the former— strong evidence that SOC is at the origin of the enhancement. Interestingly, few-layer samples also appear to possess enhanced Hc2||, with the dependence on the number of layers N being fairly weak for N >1. Due to the particular symmetries of few layer TMD crystals, this result suggests that these materials possess extremely weak interlayer coupling relative to the SOC.

Conclusions

In 2017, we performed the first measurement of the transition temperature of 1L TaS2, with Tc0 = 3 K. Our high-field measurements performed at the NHMFL point to 1L TaS2 having the highest parallel upper critical field of any intrinsically superconducting TMD. Furthermore, these measurements suggest that TaS2 may be an excellent candidate for topological and/or triplet superconductivity in two dimensions.

Acknowledgements

A portion of this work was performed at the National High Magnetic Field Laboratory, which is supported by National Science Foundation Cooperative Agreement No. DMR-1157490 and the State of Florida. Funding for SCB was provided by the Charles E. Kaufman Foundation via Young Investigator research grant KA2016-85226.  Work on device fabrication was supported by the Department of Energy Early Career program under award number DE-SC0018115.

References

[1]   de la Barrera, S.C., et al., in review.

[2]	Xi, X., et al., Nature Physics 12, 139 (2016).

[3]	Tinkham, Introduction to Superconductivity, Dover (1996).

# Text boxes

Fig.1 Upper critical field in the parallel orientation for (left) 1, 3, 4, and 5-layer TaS2 and (right) 2-layer NbSe2. Triangles show 1-layer NbSe2 data from Ref. [2]. Field axes are normalized to the paramagnetic limit, HP =1.84Tc0 [T/K], about 5.5 T for both 1-layer materials. Dashed line shows a fit to the 1L data using a standard pair-breaking theory [3], allowing extrapolation to lower temperatures and higher fields (outside the field range of cells 9 and 12).