Zeeman Splitting and Valley Populations of High Mobility Holes in WSe2

Movva, H.C.P., Fallahazad, B., Larentis, S., Tutuc, E. (Microelectronics Research Center, Department of Electrical and Computer Engineering, The University of Texas at Austin)

Introduction

Layered semiconducting transition metal dichalcogenides such as MoS2 and WSe2 represent an interesting platform for studying phenomena associated with electron-electron interactions thanks to their large effective mass carriers and strong spin-orbit coupling. We have previously demonstrated the quantum Hall effect in hole-doped mono- and bilayer WSe2, thanks to the ease of injecting holes using Pt contacts [1].

Experimental

In the past year, we further explored magnetotransport in dual-gated h-BN encapsulated mono-, bi-, and trilayer WSe2 samples [Fig. 1(a)]. Magnetotransport measurements in magnetic fields up to B = 35 T and temperatures down to T = 0.3 K were conducted using the Cell 12 resistive magnet at NHMFL in Tallahassee, FL.

Results and Discussion

We uncovered an interesting density-dependent quantum Hall states (QHS) sequence in mono- and bilayer WSe2, which transitions between predominantly even and odd filling factors as the hole-density (p) is varied [2]. The QHS transitions are due to a density-dependent g-factor which is enhanced over the band g-factor (gb) as p is reduced. Figure 1(b) shows the monolayer WSe2 effective g-factor (g*) as a function of the inter-particle distance measured in effective Bohr radius (rs). Furthermore, we also probed the valley populations of holes in trilayer WSe2. Figure 1(c) shows the longitudinal (Rxx), and Hall (Rxy) resistance vs B and the Rxx Fourier transform (FT) in trilayer WSe2, which show a beating pattern in the Shubnikov-de Haas (SdH) oscillations and two corresponding FT peaks, indicative of holes populating two subbands, associated with the K and Γ valleys [3].

Conclusions

We studied magnetotransport in mono- and bilayer WSe2 where we observed electron-electron interaction enhanced Zeeman splitting, and in trilayer WSe2 where we observed tunable Γ-K valley hole populations.

Acknowledgements

The authors acknowledge support from National Science Foundation Grant No. EECS-1610008, Intel Corp., and the Nanoelectronics Research Initiative SWAN center. A portion of this work was performed at the National High Magnetic Field Laboratory, which is supported by National Science Foundation Cooperative Agreement No. DMR-1157490 and the State of Florida.

References

[1] Fallahazad, B., et al., Phys. Rev. Lett. 116, 086601 (2016).                        [3] Movva, H. C. P., et al., Submitted.

[2] Movva, H. C. P., et al., Phys. Rev. Lett. 118, 247701 (2017).

# Text boxes

Fig.1 (a) Schematic cross section (top) and optical micrograph (bottom) of an h-BN encapsulated WSe2 Hall bar sample. (b) Monolayer WSe2 |g*| vs rs (bottom axis) or p (top axis) extracted from four samples (symbols), along with quantum Monte Carlo (QMC) calculation (solid line) using gb = 8.5. The shaded regions represent the error bars. The symbols within a group are vertically offset for clarity. (c) Trilayer WSe2 Rxx and Rxy vs B (top) at p = 8.0×1012 cm-2 and T = 0.3 K show a beating pattern of the SdH oscillations, indicative of hole population in multiple subbands. The FT spectrum (bottom) shows two principal peaks which originate from holes populating the K and Γ valleys of the valence band.