Probing the Surface of γ-Al2O3 by Oxygen-17 Dynamic Nuclear Polarization Enhanced Solid-State NMR Spectroscopy

Wang, Q. and  Xu, J. (Wuhan Institute of Physics and Mathematics, CAS, China); Gan, Z. and Mentink-Vigier, F. (NHMFL)

Introduction

γ-Al2O3 is of great importance in heterogeneous catalysis, which is widely applied either itself as catalysts or supports a wide range of important industrial reactions.  DNP-surface-enhanced NMR spectroscopy (DNP-SENS) enables atom-molecule level surface characterizations with enhanced spectral sensitivity and contrast of various materials.1 In this report, we show that surface and sub-surface oxygen species of γ-Al2O3 can be detected by 17O DNP-SENS. 1H/17O hetero-nuclear correlation (HETCOR) experiment with DNP enhancement is performed to differentiate protonated and non-protonated oxygen species.

Experimental

17O enriched of γ-Al2O3 samples (with a BET surface area of 110 m2/g) were prepared using 70%-17O2 gas according to previously reported method on oxides.2 DNP-enhanced magic-angle spinning NMR experiments were performed using the 14.1 T (600 MHz) DNP spectrometer equipped with a 3.2 mm low-temperature MAS probe at the NHMFL.

Results and Discussion

Dehydrated 17O enriched γ-Al2O3 samples were wetted with solution of biradical TEKPol in water-free and oxygen-free 1, 1, 2, 2-tetrachloroethane (C2Cl4H2) solvent for DNP measurement. Figure 1 presents the 1H MAS NMR spectra with and without microwave irradiation at ~100K showing an enhancement factor of ca. 20. With the proximity between DNP radicals to the surface, DNP enhanced spectra through either direct DNP or via cross-polarization from protons show predominantly oxygen species on and near the surface (Fig. 2). The peak in the CP spectrum agrees with the 2D 1H→17O HETCOR spectrum and we identify the peak near 0 ppm as the protonated surface oxygen species of hydroxyl groups (Fig. 3). It is interesting to note that the direct DNP spectrum shows a peak near 50 ppm. We tentatively identify as sub-surface oxygen species of γ-Al2O3 without bonded protons or bare oxygen species.

Conclusions

The complex (sub-) surface oxygen species on γ-Al2O3 were probed by 1D and 2D 17O DNP-surface-enhanced NMR spectroscopy. The large signal enhancement allows us to perform fast 1H→17O HETCOR experiments for the identification of sub-surface oxygen species.

Acknowledgements

This work was supported by the National Natural Science Foundation of China (grants 21622311, 21733013 and 21210005) and, NIH P41GM122698.  A portion of this work was performed at the NHMFL, which is supported by NSF Cooperative Agreement No. DMR-1157490 and the State of Florida.

References

[1]	Lesage, A., et al., J. Am. Chem. Soc., 132, 15459-15461(2010).

[2]	Hope, M.A., et al., Chem. Commun., 53, 2142-2145 (2017).

# Text boxes

Fig.3 2D 1H→17O HETCOR DNP spectrum of γ-Al2O3.

Fig.2 17O CP MAS NMR spectrum (top) and single pulse spectrum (bottom) of dehydrated γ-Al2O3 with DNP enhancement.

Fig.1 1H MAS NMR spectra of dehydrated γ-Al2O3 with microwave irradiation on (top) or off (bottom).