Magnetostructural Phase Diagram of Multiferroic (ND4)2FeCl5.H2O

Musfeldt, J.L., Clune, A., Hughey, K. (Tennessee); Tian, W., Fernandez-Baca, J. (Oak Ridge); Singleton, J. (Los Alamos)

__________________________________________________________________________________________

Introduction

Spin and polarization flop transitions are fascinating, especially when controlled by external stimuli like magnetic and electric field and accompanied by large material responses involving multiple degrees of freedom. Multiferroics like MnWO4, TbMnO3, and Ni3TeO6 are flagship examples and owe their remarkable properties, for instance field control of polarization and polarization flops combined with spin helix reorientation, to the anisotropy and heavy centers that bring in spin-orbit coupling. The family of A2FeX5.H2O erythrosiderites (A = K, Rb, NH4; B = Fe, Mn, Co; X = Cl, Br, H2O) drew our attention due to the rich chemical tuning possibilities, complex phase diagrams, and topological similarities to oxide multiferroics.1 (NH4)2FeCl5.H2O is the flagship example (Fig. 1(a)). It displays a high temperature order-disorder transition involving long-range hydrogen bonding of the NH4+ group and two successive low temperature magnetic transitions below which non-collinear magnetic order and ferroelectricity are established.1 In addition to the magnetically-induced electric polarization that arises below 6.9 K (P = 3 μC/m2 along a and a smaller component along b), applied field reveals a peculiar hysteretic spin flop transition near 4.5 T above which polarization flops from the a- to the c-axis.1 There are elastic components as well. Taken together, these findings raise questions about the interactions that induce this behavior and whether additional non-equilibrium phases might be accessed under even higher magnetic fields.

Results and Discussion

In order to deepen the understanding of spin-charge mixing in magnetically-driven multiferroics, we recently carried out high field magnetization measurements of (NH4)2FeCl5.H2O  and the deuterated analog at 0.6 K and 65 T at the National High Magnetic Field Laboratory in Los Alamos (Fig. 1(b)). In addition to revealing the two-component nature of the spin-flop transition from the derivative of M(B) (dovetailing perfectly with on-going inelastic neutron scattering measurements (Fig. 1(c)), these experiments uncover a magnetic quantum phase transition near 30 T. The latter is anisotropic. A preliminary magnetic field-temperature phase diagram for B ‖ a is shown in Fig. 1(d). An analysis of the critical exponents is on-going.

Fig. 1: (a) Crystal structure of (ND4)2FeCl5.D2O. (b) Pulsed field magnetization at temperatures above and below the ordering transition. (c) B – T phase diagram of (ND4)2FeCl5.D2O drawing together the low field magnetization data and inelastic neutron scattering to reveal the magnetoelectric response. (d) Developing B – T phase diagram of (ND4)2FeCl5.D2O at higher fields revealing the 30 T magnetic quantum phase transition.2

Acknowledgements

This research is supported by DMR-1707846 from the National Science Foundation and the Materials Research Fund at the University of Tennessee. A portion of this work was performed at the National High Magnetic Field Laboratory, which is supported by National Science Foundation Cooperative Agreement No. DMR-1157490 and the State of Florida.  We also appreciate funding from the Department of Energy “Science in 100 T” program.

References

[1] Ackermann, M. et al., New. J. Phys. 15, 123001 (2013).

[2] Clune, A. J. et al., to be submitted.