Thermal expansion measurements of CeRhIn5 under high pressures

Rosa, P.F.S. (MPA-CMMS, MSC); Jaime, M. (MPA-CMMS, NHMFL) and Thompson, J.D. (MPA-CMMS, MSC)

Introduction

Unconventional superconductivity can be often driven in the phase diagram of antiferromagnetic (AFM) systems when the Néel temperature (TN) extrapolates to T = 0, i.e., to a quantum critical point (QCP), as a function of chemical substitution and/or applied pressure. In particular, CeRhIn5 is a member of the heavy-fermion family CeMIn5 (M = Co, Rh, Ir) and displays AFM order at TN = 3.8 K at ambient pressure. Pressurizing CeRhIn5 suppresses TN and a superconducting dome emerges around its QCP at Pc2 = 2.35 GPa [1]. Thermal expansion (α) measurements under pressure will be key to obtaining a quantitative measure of the quantum critical scaling via the determination of the Grüneisen ratio (Γ ~ α/C, where C is the known heat capacity).

Experimental

The 20T system at Los Alamos was used for the experiments in this report.  This experiment involved the development of a new capability, and therefore we started by measuring CeRhIn5 using the Fiber Bragg Grating (FBG) technique at zero field. We obtained for the first time the a-axis thermal expansion of CeRhIn5 under hydrostatic pressures to 2 GPa and in 3He temperatures.

Results and Discussion

Figure 1a shows a picture of the setup containing two FBG sensors and a long piece of lead (manometer). One FBG sensor contains CeRhIn5 and the other one acts as a reference (no sample). The evolution of the FBG sensors as a function of applied pressure at room temperature is shown in Figure 1b. Figures 3c and 3d show the a-axis ΔL/L as a function of temperature at 0.5 GPa and 2 GPa, respectively. Anomalies at TN = 3.9 K and Tc = 2K mark the onset of the antiferromagnetic and superconducting states, respectively, and agree with the well-known phase diagram of CeRhIn5 under pressure.

Conclusions

We have implemented an optical technique for measuring thermal expansion and magnetostriction at cryogenic temperatures and under applied pressures to 2 GPa.  We demonstrate this optical approach in an a-axis sample of CeRhIn5, a heavy-fermion superconductor under applied pressure. Our results show the possibility of performing high-resolution thermal expansion measurements under pressure and open new possibilities for a broad range of materials.  A detailed description of this technique can be found in Ref. [], and an overview of recent magnetostriction measurements using FBG sensors can be found in [].

Acknowledgements

A portion of this work was performed at the National High Magnetic Field Laboratory which is supported by National Science Foundation. Work at Los Alamos was performed under the auspices of the U.S. Department of Energy, Office of Basic Energy Sciences, Division of Materials Science and Engineering.

References

[1]	T. Park et al., Nature 440, 65-68 (2006).

[2]   P.F.S. Rosa et al., Sensors 17, 2543 (2017).

[3]   M. Jaime et al., Sensors 17, 2572 (2017).

# Text boxes

Figure 1. a) Picture of the optical setup under pressure. b) Spectra of two FBG sensors at room-temperature as a function of applied pressure. c) dL/L vs T for CeRhIn5 at 0.5 GPa. Inset shows the linear thermal expansion coefficient, α (T). d) dL/L vs T for CeRhIn5 at 2 GPa. Inset shows the linear thermal expansion coefficient, α (T).