Magnetoelastic Correlations in the URu2-xFexSi2 System: Magnetostriction Measurements in Pulsed Magnetic Fields.

Breindel, A.J., Pouse, N., and Maple, M.B. (UC San Diego, Physics), Jaime, M. (NHMFL, LANL)

Introduction

Compounds which contain partially filled d- or f-electron shells can exhibit strong electronic correlations from the hybridization of the localized d- or f-electron and conduction electron states. This hybridization often leads to the emergence of new electronic ground states such has complex magnetic order, quadrupolar order, non-Fermi liquid behavior and unconventional superconductivity [1]. One example of such exotic ordering behavior is the “hidden-order” phase of URu2Si2, the order parameter of which has been a mystery for decades.  When iron is substituted into the ruthenium site, URu2Si2 has been demonstrated behave in a way that is a strong analogue for applied pressure on the system, allowing the system to be probed as though it were under pressure in experiments where it would be difficult to do so [2]. Magnetostriction using Fiber Bragg Grating (FBG) dilatometry is one such experiment, which is able to probe the phase transitions of the material in new and interesting ways, and may help to provide some insight into the hidden order phase [3].

Experimental

Our experiment was conducted in a 65 Tesla pulsed magnet at NHMFL, using a FBG dilatometry probe made for use in these magnets. This probe allowed us to measure the magnetostriction of the sample at various temperatures.

Results and Discussion

This was a repeat attempt at an experiment which had previously largely failed, believed to be because of the large cross-sectional area of the samples causing a stronger than anticipated interaction with the magnetic field. Pleasingly, this attempt, which used smaller samples, was significantly more successful, with Figures 1 and 2 showing example data. Each figure shows the magnetostriction data at various temperatures, and clear signs of phase transitions are present. These phase transitions can be tracked to inform us about the overall phase diagram for this system and relative strength of magnetoelastic couplings.

Acknowledgements

A portion of this work was performed at the National High Magnetic Field Laboratory, which is supported by National Science Foundation Cooperative Agreement No. DMR-1157490 and the State of Florida.

Research at UCSD was supported by the US DOE BES under Grant No. DE-FG02-04-ER46105 (materials synthesis and characterization), the US NSF under Grant No. DMR-1206553 (low temperature measurements), and the NNSA under the SSAA program through the US DOE under Grant No. DE-NA0002909 (high field measurements)

References

[1] Maple, M. B., et al., Low Temp. Phys, 161, 4 (2010).

[2] Kanchanavatee, N., et al., Phys. Rev. B 84, 245122 (2011).

[3] Jaime, M., et al., Sensors 17, 2572 (2017).

# Text boxes

Fig.2 Magnetostriction data at various temperatures. For URu2-xFexSi2 x = 0.2. Data is offset for clarity

Fig.1 Magnetostriction data at various temperatures. For URu2-xFexSi2 x = 0.1. Data is offset for clarity