Directional Dichroism of THZ Radiation in the Canted AFM Phase of BiFeO3

Rõõm, T., Viirok, J., Nagel, U. (National Institute of Chem. Phys. and Biophys., Tallinn, Estonia); Farkas, D., Bordács, S., Kézsmárki, I. (BME, Budapest, Hungary); Thirunavukkuarasu, K., Krzystek, J. (NHMFL, Tallahassee); Ozaki, Y., Tomioka, Y., Ito, T. (AIST, Tsukuba, Japan)

Introduction

Multiferroics (MF) permit the magnetic control of the electric polarization and the electric control of the magnetization. These static magnetoelectric (ME) effects are of enormous interest: The ability to read and write a magnetic state current-free by an electric voltage would provide a huge technological advantage. Optical ME effects are equally interesting, because they give rise to unidirectional light propagation as recently observed in low-temperature multiferroics[1]. BiFeO3 is the only room temperature MF and has the largest spin driven polarization among MF. The material shows directional dichroism (DD) at THz frequencies even at room temperature and it is established that the optical ME effect is caused by the spin-current mechanism in the cycloidally ordered magnetic phase[2].

In the magnetic fields above 18T the spin cycloid is destroyed, accompanied by a sudden change of the electric polarization along the hexagonal axis parallel to the existing FE polarization. It has been found recently that linear ME effect exists in the canted AFM phase[3]. To unravel the mechanism of linear ME coupling in the canted AFM phase we have undertaken a study of DD above 18T in the THz range.

Experimental

Experiment was carried out in cell 8 on 35T 32mm bore magnet using quasi-optical cryostat. THz radiation was generated with backward wave oscillators and detected with hot electron bolometer operating at T=4K. Radiation was propagating perpendicular to the magnetic field (Voigt configuration).

Results and Discussion

We studied the polarization dependence of the lower AFM mode for magnetic field in three principal hexagonal directions, B||[111], B||[1-10] and B||[-1-12], given in pseudo-cubic notation. The result for B||[-1-12] is shown in figure 1. The lower AFM mode shows DD as shown in figure 2.

Conclusions

We detected DD and determined the selection rules for the lower AFM mode.

Acknowledgements

A portion of this work was performed at the National High Magnetic Field Laboratory, which is supported by National Science Foundation Cooperative Agreement No. DMR-1157490 and the State of Florida and some parts of the work by the Estonian Ministry of Education and Research (IUT23-3) and Estonian Ministry of Education and Research and the European Regional Development Fund project TK134.

References

[1]	Kézsmárki, I., et al., Nature Communications, 5, 3203 (2014).

[2]	Kézsmárki, I., et al., Phys. Rev. Lett., 115, 127203 (2015)

[3]	Tokunaga, M., et al., Nature Communications 6, 5878 (2015)

Fig.  2: Lower AFM spectra showing DD

Fig.  1: Polarization dependent modes for the B||[-1-12] direction