High Field Studies of Magnetic Weyl Semimetals

Ye, L. (MIT, Physics); Suzuki, T. (MIT, Physics); Devarakonda, A. (MIT, Physics); Checkelsky, J.G. (MIT, Physics)

Introduction

The search for the overlap of electron correlation and electronic topology has led to the exploration of materials with strong spin-orbit coupling and magnetic ordering.  The rare-earth monopnictide CeSb is a correlated material with more than 10 distinct magnetic ground states in its low temperature – magnetic field phase diagram.  As such, it is an interesting platform to explore the mapping of a variety of magnetic ground states on to a system of strongly spin-orbit coupled electrons to look for new phenomena potentially connected to electronic topology.

Experimental

Single crystals of CeSb were grown by a flux method. Transport measurements were performed at the NHMFL DC Field facility in a He3 cryostat in Cell 9. Longitudinal resistivity data is shown here.

Results and Discussion

The longitudinal electrical resistivity ρxx as a function of magnetic field along the [001] direction is shown in Fig.1.  At low magnetic field a number of sharp features are observed associated with the successive magnetic phase transitions expected on CeSb [1].  Upon reaching the high field ground state at all temperatures, a large magnetoresistance is observed.  Particularly at low temperatures, this evolves in to a non-saturating MR reaching large values consistent with XMR [2].  XMR has recently been identified a number of non-magnetic topological semimetals [3]- the origin of this effect may be related to near perfect compensation in these systems.  If such connections are relevant to CeSb and the related rare-earth monopnictide family are now the subject of ongoing investigation.  In particular, the non-saturating behavior observed here to 31 T puts a strong constraint on the level compensation required and may stand as a test for theoretical models for the electronic structure of these correlated materials.

Conclusions

We studied the high field magneto-transport properties of CeSb.  Despite the complex phase diagram, for sufficient fields above 20 T XMR is seen across the entire low temperature range.

Acknowledgements

A portion of this work was performed at the National High Magnetic Field Laboratory, which is supported by National Science Foundation Cooperative Agreement No. DMR-1157490 and the State of Florida.

In addition, this research is funded in part by the Gordon and Betty Moore Foundation EPiQS Initiative, Grant GBMF3848 to J.G.C., material development by NSF grant DMR-1554891, and instrumentation development with ARO grant W911NF-16-1-0034. L.Y. acknowledges support by the STC Center for Integrated Quantum Materials, NSF Grant No. DMR-1231319 and by the Tsinghua Education Foundation. J.G.C. acknowledges support from the Bose Fellows Program at MIT.

References

[1] 	Rossat-Mignod, J., et al., J. Magn. Magn. Mater. 31-34, 398-404 (1985).

[2]	Ye, L., et al., arXiv: 1704.04226 (2017).

[3]	Tafti, F. F, et al., Proc. Nat. Acad Sci 113, E3475-E3481 (2016).

# Text boxes

Fig.1 Magnetoresistance of CeSb to magnetic field 31 T showing XMR