Light-Induced Magnetization Changes in Aggregated and Isolated

Cobalt Ferrite Nanoparticles

Brinzari*, T.V. (UF, Physics); Rajan*, D. (UF, Chemistry); Ferreira, C.F. (UF, Chemistry); Stoian, S.A. (NHMFL-Tallahassee, EMR and Univ. Idaho, Chemistry); Quintero, P.A. (UF, Physics); Meisel, M.W. (UF, Physics and NHMFL); Talham, D.R. (UF Chemistry).  * These authors contributed equally to this work.

Overview

This study reinvestigates the light-induced coercivity changes, ΔHC ( 3 kOe at 10 K, in cobalt ferrite (CoFe2O4) nanoparticles first reported by Giri et al. [1,2]  Motivated by renewed interests in photo-controlled magnetic response, our work presents a more comprehensive set of analyses of the photomagnetic effects in cobalt ferrite nanoparticles [3].  In addition to the light-induced coercivity changes communicated by Giri et al. [1,2], we observed changes in the remanent magnetization and the magnetization in 70 kOe upon irradiation with light, Fig. 1.  Further experimental evidence suggests the mechanism of the effect goes beyond an optically triggered charge transfer.  The photo-effects are found to depend on the sample preparation, with aggregates of nano-particles formed by coprecipitation (Copt) showing a significantly larger effect than isolated nanoparticles formed by thermal decomposition (TD).  Field and temperature dependent magnetometry data implicate the interaction of light with spins at the surface of the particles as a likely origin of the novel behavior.

Experimental Details

The synthesis protocols are described elsewhere [3].  The samples were subjected to a suite of probes, including magnetometry, X-ray photoelectron spectroscopy, and 57Fe Mössbauer spectroscopy performed in the NHMFL EMR facility.

Results and Discussion

The full set of results and the associated discussion are found elsewhere [3].  Figure 1 presents the data for the magnetization results for three samples summarized in Table 1.

| Sample | Synthesis Protocol | Overall Form | Mesoscale Size (nm) | Nanoscale Size (nm) |
| --- | --- | --- | --- | --- |
| 1 | Copt | Aggregate | 270 ± 90 | 7 ± 2 |
| 1a | Copt | Aggregate | 265 ± 90 | 17 ± 5 |
| 2 | TD | Isolated | --- | 6 ± 1 |

Table 1.  Summary of the characteristics of the samples shown in Fig. 1.  See Ref. [3] for complete details.

Acknowledgements

This work was supported by the NSF via DMR-1405439 (D.R.T.), DMR-1202033 and DMR-1708410 (M.W.M.), and by the University of Florida Office of Research.  A portion of this work was performed at the NHMFL, which is supported by the NSF via Cooperative Agreement DMR-1157490 and the State of Florida.  One author (S.A.S.) acknowledges partial support from the NHMFL Jack E. Crow Postdoctoral Fellowship.  This research used resources of the Advanced Photon Source, a U.S. DOE Office of Science User Facility operated for the DOE Office of Science by Argonne National Laboratory.  We thank C.R. Gros, A.A. Ahir, A. Felts, and G.H. Halder for assistance.

References

[1]	Giri, A., et al., IEEE Trans. Magnetics, 36, 3029-3031 (2000).

[2]	Giri, A., et al., Applied Physics Letters, 80, 2341-2343 (2002).

[3]	Brinzari, T.V., Rajan, D., et al., submitted (2017).

Figure 1.  Magnetization versus applied magnetic fields as measured in the dark and light states at 10 K for (a) Sample 1, (b) Sample 1a, and (c) Sample 2.  Insets at the bottom right of each figure are the TEM micrographs of the respective samples and the ones at the top left of each panel provide an expanded view of the low field regions.