Spin susceptibility of charge ordered YBa2Cu3Oy across the upper critical field

Zhou, R., Hirata, M., Wu, T., Vinograd, I., Mayaffre, H., Krämer, S., Julien, M.-H. (LNCMI-EMFL Grenoble);

Reyes, A.P., Kuhns, P.L. (NHMFL) ; Hardy, W.N., Liang, R., Bonn, D.A. (University of British Columbia, Vancouver)

Introduction

The upper critical field Hc2 is a fundamental, and technologically important, property that measures the

ability of a superconductor to withstand magnetic fields. Recently, there has been a controversy regarding Hc2  values in high-Tc  copper-oxides. The dispute has become particularly acute in the context of the competition between superconductivity and charge density wave (CDW) order in underdoped YBa2Cu3Oy. Since the issue has been tackled almost exclusively by macroscopic techniques so far, there is a clear need for local-probe measurements.

Experimental

We have used NMR to measure the field dependence (up to 45 T on the NHMFL hybrid magnet) of the spin susceptibility χspin at low temperature (T) in charge ordered YBa2Cu3Oy. More specifically, we have measured the total 17O Knight shift in four different crystals and have determined its spin part Kspin, proportional to χspin of the CuO2  planes, by subtracting the orbital contribution, while the contribution from diamagnetic shielding was found to be negligible at the fields used. Even though in the cuprates, χspin is in general not related to N(EF) in a simple way, we expect the field dependence of χspin at low T  to reflect the field-dependence of N(EF).

Results and Discussion

The central result of this study is the observation of an essentially linear increase in χspin up to a point in the range of 20 to 40 T, followed by a constant value. This saturation point agrees quantitatively with Hc2 values claimed in [G. Grissonnanche et al., Nat. Commun. 5, 3280 (2014)], showing a very large depression around p = 0.12 doping (Fig.1). Our data further show that a large pseudogap persist above Hc2 in the zero-temperature limit and that χspin is insensitive to the onset of three-dimensional long-range charge-density-wave (CDW) order.

Conclusions

Our results [1] show that short-range CDW order (already present in zero field) reconstructs the Fermi surface and reduces Hc2 in underdoped YBa2Cu3Oy. They also show that the pseudogap is a ground-state property, independent of the superconducting gap.

Acknowledgements

A portion of this work was performed at the National High Magnetic Field Laboratory, which is supported by National Science Foundation Cooperative Agreement No. DMR-1157490 and the State of Florida.

Work in Grenoble was supported by the French Agence Nationale de la Recherche (ANR) under reference AF-12-BS04-0012-01 (Superfield) and by the Laboratoire d’Excellence Laboratoire d’Alliances Nanosciences – Energies du Futur (LANEF) in Grenoble (ANR-10-LABX-51-01). Work in Vancouver was supported by the Canadian Institute for Advanced Research and the Natural Science and Engineering Research Council.

References

[1]	Zhou, R., et al., PNAS, 114, 13148–13153 (2017).

# Text boxes

Fig.1 Saturation field in Knight shift measurements (blue dots, this work) at T ~ 2 K, compared to Hc2 values extrapolated to T = 0 from resistivity data [B. Ramshaw et al., Phys. Rev. B 86, 174501 (2012)].