Fermi surface and Berry phase in CaFeAsF, a variant of the 1111 parent compounds

Terashima, T.; Hirose, H.T.; Uji, S. (NIMS); Graf, D. (NHMFL); Ma, Y.; Mu, G.; Hu, T. (Shanghai Institute of Microsystem and Information Technology); Suzuki, K.; Ikeda, H. (Ritsumeikan Univ.)

Introduction

Despite the fact that 1111-type iron arsenides hold the record transition temperature of iron-based superconductors, their electronic structures have not been studied much because of the lack of high-quality single crystals.  Recently, Ma et al. have succeeded in growing large high-quality single crystals of CaFeAsF [1].  We have performed Shubnikov-de Haas (SdH) measurements on those crystals [2].

Experimental

We have performed standard four-contact resistivity measurements using a 20-T superconducting magnet at the NIMS and the 45-T Hybrid Magnet at the NHMFL.

Results and Discussion

Figure 1(a) shows the field derivative of magnetoresistivity for B // c (inset) and corresponding Fourier transform, where two frequencies α and β are resolved.  Their field-angle dependences indicate that they are from two-dimensional cylinders.  The carrier density is extremely small, ~10-3 per Fe.  The effective masses are estimated to be 0.383 and 0.92 me from the temperature dependences of the oscillations.  We now determine the Berry phase.  The SdH oscillation is given by Δρ = −C Rs cos [2π(F/B − 1/2) + φD + φB], where C is a positive factor, φD = 0 (2D) or +/-π/4 (3D).  When the double degeneracy of electronic bands due to spin degrees of freedom exits, which is the case for CaFeAsF, it is necessary to determine the sign of the spin reduction factor Rs = cos (πgμ*/2), where μ* = m*/me, before the Berry phase φB (sign change in Rs is equivalent to a π phase shift).  Figure 1(b) shows the analysis for the α oscillation.  Plotted are the oscillatory part of resistivity after box-smoothing with a window size corresponding to one period of the β oscillation.  The smoothing suppresses the β oscillation effectively, and the remaining oscillatory behavior is basically due to the α oscillation.  Near Fα/B = 2, a minimum is observed for θ ≤ 48.3°, while a maximum for θ ≥ 57.4°.  Assuming μ*(θ) = μ*(0)/cos θ, this observation indicates that 1.41 < g < 1.73.  For this range of g, Rs > 0 at θ = 0.  Since Δρ at θ = 0 shows a minimum near Fα/B = 2, the Berry phase is determined to be π (see the above formula), i.e., the α carriers are Dirac fermions.  A similar analysis for the β oscillation indicates that the β carriers are normal fermions.  Our band-structure calculation indicates that the Fermi surface consists of a pair of Dirac electron cylinders and a normal hole cylinder, corresponding nicely to the experimental α and β cylinders, respectively.

Conclusions

We have determined the Fermi surface in CaFeAsF completely and also demonstrated a nontrivial Berry phase associated with the α oscillation.

Acknowledgements

A portion of this work was performed at the National High Magnetic Field Laboratory, which is supported by National Science Foundation Cooperative Agreement No. DMR-1157490 and the State of Florida.

This work was supported by JSPS KAKENHI Grant Numbers JP17K05556, 17J06088, 16H04021, 16H01081, and the Youth Innovation Promotion Association of the Chinese Academy of Sciences (No. 2015187).

References

[1]	Ma, Y., et al., Supercond. Sci. Technol. 28, 085008 (2015).

[2]	Terashima, T., et al., arXiv:1710.03938.

# Text boxes

Fig.1 (a) Field-derivative of magnetoresistivity for B // c (inset) and corresponding Fourier transform.  (b) Oscillatory part of resistivity after box-smoothing with a window size corresponding to one period of the β oscillation plotted against 1/Bcosθ.  θ is the field angle measured from the c axis.  Data for θ = 47.7° and θ ≥ 52.6° were obtained with the Hybrid.