Fermi surface and electrical transport properties of the topological semimetal candidates (Nb,Ta)IrTe4

Schoenemann, R. and Balicas, L. (National High Magnetic Field Laboratory)

Introduction

NbIrTe4 belongs to the family of non-centrosymmetric van der Waals stacked layered transition metal dichalcogenides (space group Pmn21) that has been recently predicted to be topological Weyl semimetal in the bulk and a quantum spin Hall insulator in the monolayer [1]. Here we show preliminary results of measurements of the Shubnikov-de Haas (SdH) effect and effective charge carrier masses in this material.

Experimental

AC transport experiments have been conducted in a 3He cryostat in cell 12 up to 34.5 T using a rotator probe. A conventional four terminal method was used to measure the sample resistance.

Results, Discussion and Conclusion

SdH oscillations in NbIrTe4 have been observed for fields parallel to the crystallographic c-axis and ab-plane for several temperatures (Fig. 1). We were able to extract effective masses from fitting the amplitude of the FFT peaks as a function of temperature with the temperature damping factor of the Lifshitz-Kosevitch formula for 2 frequencies of each orientation. NbIrTe4 exhibits relatively light effective masses in the range of 0.3 to 1 electron masses and shows several distinct frequencies for both, c-axis and ab-plane orientations. Our goal is therefore a future study of the full angular dependence of the SdH oscillations that can be compared to band structure calculations and predictions of Weyl physics.

Acknowledgements

This work was supported by DOE-BES through Award N. DE-SC0002613. A portion of this work was performed at the National High Magnetic Field Laboratory, which is supported by National Science Foundation Cooperative Agreement No. DMR-1157490 and the State of Florida.

References

[1]	Liu, J., et al., Nano Letters, 17, 467-475 (2017).

# Text boxes

Fig.1 (a) Resistance vs. field of a NbIrTe4 single crystal for H II c, the inset shows the oscillatory signal after background subtraction. (b) and (d) show the Fast Fourier Transform (FFT) of the SdH oscillations for fields along the c-axis and ab-plane. The respective FFT amplitudes as a function of temperature and the extracted effective masses for both orientations are displayed in (c) and (e).