## Slide 1
Since their discovery in 2008, the iron-based superconductors have been studied extensively because of their high superconducting transition temperatures (TC). Despite the fact that the TC record of 56 K is held by a 1111-type iron arsenide, little is known about the electronic structure of these compounds. These experiments on CaFeAsF revealed the electronic structure (i.e. the Fermi surface) of a parent 1111 compound, a compound that becomes superconducting upon doping, thus providing valuable insight into how super-conductivity emerges in this family of 1111-type iron-based superconductors.
This three-nation collaboration performed angular-dependent electrical transport measurements on CaFeAsF in magnetic fields up to 45T and at temperatures down to 0.3K. Quantum oscillations were clearly observed, revealing that the Fermi surface consists of both electron and hole cylinders. The carrier density was found to be anomalously low, and the electron carriers were found to possess a nontrivial Berry phase of π. This indicates that these electrons are relativistic quasiparticles, that is, Dirac fermions.
These results proved a first picture of the electronic structure of a parent compound of 1111-type iron-based superconductors. Furthermore, they suggest a new avenue to explore Dirac-fermion physics in iron-based superconductors.
Figure: (Top) Quantum oscillations in CaFeAsF, observed as oscillations in the electrical resistivity plotted against 1/(Bcosθ) (bottom axis), where B is magnetic field and θ is the angle between the magnetic field and the crystalline c axis. (Bottom) Fermi surface of CaFeAsF, which represents the momenta of the highest-energy electrons in the material. The left inset shows a part of the electronic band dispersions, showing a linear dependence of the electon’s energy versus momentum. These Dirac electrons exist where the blue and red bands cross to produce the green electron cylinders of the Fermi surface.
Dirac Fermions Detected via Quantum Oscillations
T. Terashima,1 H. T. Hirose,1 D. Graf,2 Y. Ma,3,4 G. Mu,3,4 T. Hu,3,4 K. Suzuki,5 S. Uji,1 and H. Ikeda5
1. NIMS, Japan; 2. NHMFL, FSU; 3. SIMIT, China; 4. CENSE, CAS, China; 5. Ritsumeikan U., Japan
Funding Grants: G.S. Boebinger (NSF DMR-1157490); T. Terashima (JSPS KAKENHI JP17K05556);
G. Mu (Youth Innovation Promotion Association of CAS No. 2015187); T. Hu (National Natural Science Foundation
of China No.11574338); H. Ikeda (JSPS KAKENHI JP17J06088, JP16H04021, JP16H01081)
45
Facilities and instrumentation used: DC Magnet User Facility: 45 Tesla, 32 mm Bore Hybrid Magnet, He-3 Cryogenic System.
Citation: T. Terashima, H.T. Hirose, D. Graf, Y. Ma, G. Mu, T. Hu, K. Suzuki, S. Uji, and H. Ikeda, Fermi Surface with Dirac Fermions in CaFeAsF Determined via Quantum Oscillation Measurements, Physical Review X 8, 011014 (2018) , DOI: 10.1103/PhysRevX.8.011014

## Slide 2
What is the finding? The Fermi surface provides information about which electrons determine many of the properties of a given metal, including its electrical resistivity. This collaboration succeeded in completely determining the Fermi surface of a material, CaFeAsF, that is interesting because it is a parent compound from which “1111-type” iron-based superconductors are made. This Fermi surface mapping resulted from measuring the quantum oscillations in the electrical resistance that occur as the magnetic field is swept and rotated [top figure]. These measurements demonstrated that some of the electrons on the Fermi surface in CaFeAsF are Dirac fermions.
Why is this important? Among the many families of iron-based super-conductors, the 1111-type features the highest superconducting transition temperature, but progress has been limited due to sample quality issues. This first observation of the Fermi surface in a type-1111 compound significantly improves our understanding of these materials, including establishing the existence of Dirac fermions, which may enable future industrial applications.
Why did this research need the MagLab? The MagLab’s unique combination of ~0.3K temperatures and 45T magnetic fields was needed to reveal quantum oscillations in this 1111-type material.
Figure: (Top) Quantum oscillations in CaFeAsF, observed as oscillations in the electrical resistivity plotted against 1/(Bcosθ) (bottom axis), where B is the magnetic field and θ is the angle between the magnetic field and the crystalline pointing up in the bottom figure. (Bottom) Fermi surface of CaFeAsF, which represents the momenta of the highest-energy electrons in the material. The left inset shows a part of the electronic band dispersions, showing a linear dependence of the electron’s energy versus momentum. These Dirac electrons exist where the blue and red bands cross to produce the green electron cylinders shown in the Fermi surface at the bottom right.
Dirac Fermions Detected via Quantum Oscillations
T. Terashima,1 H. T. Hirose,1 D. Graf,2 Y. Ma,3,4 G. Mu,3,4 T. Hu,3,4 K. Suzuki,5 S. Uji,1 and H. Ikeda5
1. NIMS, Japan; 2. NHMFL, FSU; 3. SIMIT, China; 4. CENSE, CAS, China; 5. Ritsumeikan U., Japan
Funding Grants: G.S. Boebinger (NSF DMR-1157490); T. Terashima (JSPS KAKENHI JP17K05556);
G. Mu (Youth Innovation Promotion Association of CAS No. 2015187); T. Hu (National Natural Science Foundation
of China No.11574338); H. Ikeda (JSPS KAKENHI JP17J06088, JP16H04021, JP16H01081)
Facilities and instrumentation used: DC Magnet User Facility: 45 Tesla, 32 mm Bore Hybrid Magnet, He-3 Cryogenic System.
Citation: T. Terashima, H.T. Hirose, D. Graf, Y. Ma, G. Mu, T. Hu, K. Suzuki, S. Uji, and H. Ikeda, Fermi Surface with Dirac Fermions in CaFeAsF Determined via Quantum Oscillation Measurements, Physical Review X 8, 011014 (2018) , DOI: 10.1103/PhysRevX.8.011014
45
Notes: 1. What is the finding?
Here to be included a short description in layman language of the finding
2. Why this finding is important?
A short description of why the finding is important for scientific community, technology, society, etc…
3. Why NHMFL?
The answer to this question should provide information on why this finding could be achieved (only) at NHMFL (what unique capability of MagLab was essential for this finding).