## Slide 1
The spin up and spin down electrons in Dirac materials, such as graphene, share a Dirac-cone in momentum space. Weyl semimetals split this degeneracy into two Weyl-nodes with opposite handedness of spin-chirality, this provides the possibility of observing new phenomena. Weyl electrons, for example, are predicted to give rise to a chiral anomaly, whereby parallel electric and magnetic fields can pump an imbalance between the Weyl nodes leading to a topologically protected current.
To date all Weyl metals not only possess Weyl electrons but also trivial electrons, complicating the search for the associated phenomena. Our solution was to use extreme magnetic fields (95 tesla) to drive the Weyl metal TaAs deep into its quantum limit where only the purely chiral zeroth Landau levels are populated, and there we observed the chiral anomaly.
This illustrates how high magnetic fields can be used to overcome material constraints and access a state composed purely of Weyl fermions, and points the way to inducing new correlated states of matter composed of these exotic quasiparticles.
Facilities: 100 tesla and 65 tesla short pulsed magnet systems.
Citation: B.J. Ramshaw, K.A. Modic, A. Shekhter, Y. Zhang, E.-A. Kim, P.J.W. Moll, M. Bachmann, M.K. Chan, J.B. Betts, F. Balakirev, A. Migliori, N.J. Ghimire, E.D. Bauer, F. Ronning, and R.D. McDonald,
Quantum limit transport and destruction of the Weyl nodes in TaAs, Nature Communications 9: 2217 (2018). DOI: 10.1038/s41467-018-04542-9
Figure (a) Resistivity of the Weyl semimetal, TaAs, for both current and magnetic field along the c-axis from T=20K to 0.7K. Quantum oscillations from the Weyl pockets are visible up to 7.5T, followed by a decrease and then saturation of the resistivity in temperature and field up to 50T. Above 50T, there is a two order-of-magnitude increase resistivity at low temperature, signifying the opening of an energy gap. The inset shows single-crystal TaAs microstructured using focused-ion-beam (FIB) lithography for both rzz and rxx measurements. (b) Change of the longitudinal sound speed measured at 315 MHz for both the sound propagation and magnetic field along the c-axis. Above 2.5K, the sound velocity flattens out above 80T and the attenuation is only weakly field dependent. Below 2.5K, however, both the sound velocity and the ultrasonic attenuation increase rapidly with field. The red line at 90T highlights the abruptness of the high-field transition as a function of temperature. The inset illustrates the hole dispersion (red), and electron-like Weyl fermions (blue), separated into distinct right and left-handed chiralities.
Destruction of Weyl nodes and a New State in TaAs above 80 Teslas
B.J. Ramshaw,1, 2 K.A. Modic,3 Arkady Shekhter,4 Yi Zhang,2 Eun-Ah Kim,2 Philip J.W. Moll,3 Maja Bachmann,3 M.K. Chan,1 J.B. Betts,1 F. Balakirev,1 A. Migliori,1 N.J. Ghimire,5, 1 E.D. Bauer,1 F. Ronning,1 and Ross D. McDonald1
1.Los Alamos National Laboratory, 2. Laboratory of Atomic and Solid State Physics, Cornell University, 3. Max-Planck-Institute for Chemical Physics of Solids, 4.National High Magnetic Field Laboratory, 5. Argonne National Laboratory
Funding Grants: G.S. Boebinger (NSF DMR-1157490, NSF DMR-1644779); B.J. Ramshaw (LANL LDRD-ECR20160616 “New States of Matter in Weyl Semimetals”); M.K. Chan (DOE-BES “Science at 100 T program”);
R.D. McDonald (LANL LDRD-DR20160085 “Topology and Strong Correlations” );
Notes: Paragraph 1: Introduction: a sentence or two on the general context of this work, comprehensible by non-experts.
Paragraph 2: Experimental description (enough detail to capture the excitement of the result, the nature of the collaboration, the capability of the MagLab facilities that enabled the success).
Paragraph 3: So what? What area of research has been advanced ? What longer term basic research and/or applications might result ?

## Slide 2
What is the finding? From 20 to 50 teslas, we find the electrical resistivity (for parallel electric and magnetic fields) to be nearly independent of magnetic field: highly unusual for a conventional metal, but consistent with the strange behavior of Weyl fermions. Above 50 teslas, we observe a two-order-of-magnitude increase in resistivity, indicating the destruction of the Weyl nodes by the opening of an energy gap. Above 80 teslas, we observe strong ultrasonic attenuation at temperatures below 2 kelvin, suggesting a new mesoscopically-textured state of matter
Why is this important? Fundamentally, strong spin-orbit coupled metals provide a wealth of new phenomena that are not known to exist outside of materials physics. The topological nature of the resulting states not only makes them robust against perturbation, but provides a possible bridge of the quantum-material to quantum-information chasm.
Why the MagLab? Multiple measurements of the conductivity, sound velocity, and attenuation above 90 tesla is only possible at the MagLab.
Facilities: 100 tesla and 65 tesla short pulsed magnet systems.
Citation: B.J. Ramshaw, K.A. Modic, A. Shekhter, Y. Zhang,
E.-A. Kim, P.J.W. Moll, M. Bachmann, M.K. Chan, J.B. Betts, F. Balakirev, A. Migliori, N.J. Ghimire, E.D. Bauer, F. Ronning, and R.D. McDonald,
Quantum limit transport and destruction of the Weyl nodes in TaAs, Nature Communications 9: 2217 (2018). DOI: 10.1038/s41467-018-04542-9
Destruction of Weyl nodes and a New State in TaAs above 80 Teslas
B.J. Ramshaw,1, 2 K.A. Modic,3 Arkady Shekhter,4 Yi Zhang,2 Eun-Ah Kim,2 Philip J.W. Moll,3 Maja Bachmann,3 M.K. Chan,1 J.B. Betts,1 F. Balakirev,1 A. Migliori,1 N.J. Ghimire,5, 1 E.D. Bauer,1 F. Ronning,1 and Ross D. McDonald1
1.Los Alamos National Laboratory, 2. Laboratory of Atomic and Solid State Physics, Cornell University, 3. Max-Planck-Institute for Chemical Physics of Solids, 4.National High Magnetic Field Laboratory, 5. Argonne National Laboratory
Funding Grants: G.S. Boebinger (NSF DMR-1157490, NSF DMR-1644779); B.J. Ramshaw (LANL LDRD-ECR20160616 “New States of Matter in Weyl Semimetals”); M.K. Chan (DOE-BES “Science at 100 T program”);
R.D. McDonald (LANL LDRD-DR20160085 “Topology and Strong Correlations” );
Figure (a) Electrical resistivity of the Weyl semimetal, TaAs, for temperatures from T=20K to 0.7K. Note the saturation of the resistivity in temperature and field up to 50T. Above 50 tesla there is a two order-of-magnitude increase resistivity at low temperature, signifying the destruction of the Weyl nodes by the opening of an energy gap. The inset shows single-crystal TaAs microstructured using focused-ion-beam (FIB) lithography.
(b) Change of the longitudinal sound speed. Above 2.5K, the sound velocity flattens out above 80T and the attenuation is only weakly field dependent. Below 2.5K, however, both the sound velocity and the ultrasonic attenuation increase rapidly with field. The red line at 90T highlights the abruptness of the high-field transition as a function of temperature. The inset illustrates the hole dispersion (red), and electron-like Weyl fermions (blue), separated into distinct right and left-handed chiralities.
Notes: What is the finding? Here to be included a short description in layman language of the finding
Why is this important? A short description of why the finding is important for scientific community, technology, society, etc…
Why did this research need the MagLab? The answer to this question should provide information on why this finding could be achieved (only) at NHMFL (what unique capability of MagLab was essential for this finding).