## Slide 1
Superconducting Hydride under Extreme Magnetic Fields and Pressure
S. Mozaffari1, L. Balicas1, V. S. Minkov2, D. Knyazev2, M. I. Eremets2,
M. Einaga3, K. Shimizu3, D. Sun4, F. F. Balakirev4
National High Magnetic Field Laboratory, Florida State University; 2. Max-Planck-Institut fur Chemie;
3. Osaka University; 4. National High Magnetic Field Laboratory, Los Alamos National Laboratory
Funding Grants: G.S. Boebinger (NSF DMR-1157490, NSF DMR-1644779); Balicas (DoE-BES DE-SC0002613); Eremets(ERC- 267777)
The BCS (Bardeen–Cooper–Schrieffer, 1957) theory of superconductivity suggests that there is room for higher superconducting critical temperatures (Tc) in metals composed of light elements (such as hydrogen). Materials with high values for both a phonon frequency and the electron-phonon coupling constant are favorable candidates in the search for a higher Tc. The recently discovered record Tc of 203 K in hydrogen sulfide at 160 GPa confirmed a major result of BCS theory for conventional (phonon-mediated) superconductors, that might for some material result in a Tc above room temperature.
Measurements of the superconducting phase-diagram under high magnetic fields provide detailed information on the underlying electron-phonon coupling. Here, we report magnetotransport studies in superconducting sulphur hydride, under extremely high pressures, in DC fields up to 35T and pulsed fields up to 65T.
We compare the measured upper critical magnetic field with the BCS formula of Werthamer, Helfand and Hohenberg (WHH), noting deviations from the WHH behavior at the lowest experimental temperatures accessible using 65T magnetic fields. The extrapolated zero-temperature upper critical field Hc2 surpasses 100T, assuming the WHH formula holds.
DC PULSED
a
b
Figure b, Superconducting
upper critical fields as a function of temperature for two samples under pressures of 150 and 170 GPa. Open markers are DC field data and solid ones are pulsed field data. For each sample, we show data for Hc2 (purple and red) and H* (light and dark blue). Solid lines are fits to the formula: Hc2 = Hc2(0)[1-(T/Tc)2].
Inset photos: the diamond anvil cell and the sample.
Figure a, Resistance as a function of magnetic field at several temperatures (T) for a sulfur hydride sample under hydrostatic pressure of 170 GPa. Red dashed lines Indicate the definition of Hc2, the upper critical magnetic field, and H*, the superconducting transition onset.
a
Facilities and instrumentation used: DC Facility 35T magnet, Pulsed Facility 65T magnet
Citation: Manuscript in preparation

## Slide 2
DC PULSED
a
What is the finding? A recent collaboration among researchers at the MagLab and the Max Plank Institute for Chemistry characterized the high-magnetic-field properties of the hydride superconductors, the latest big leap forward on the road to room temperature superconductivity. Hydrogen sulfide, a rotten egg smelling gas, first becomes metallic then becomes superconducting when squeezed between two anvils made of diamond to pressures above one million atmospheres. At pressures of 170GPa, the superconducting transition temperature achieves 203K. For comparison, these pressures are about half of those
estimated to exist at the earth’s core.
Why is this important? Superconductivity is a state of a material in which its resistance is exactly zero, i.e. an electrical current can flow without any frictional losses. The world will become a different place if room temperature superconductivity is discovered and superconductivity can replace conventional conductivity in metals where heating is a waste of energy.
Why did this research need the MagLab? High temperature superconductors require very high magnetic fields to fully understand their properties. MagLab researchers found that fields as high as 100 Tesla might not be strong enough to fully suppress superconductivity in hydrogen sulfide.
Facilities and instrumentation used: DC Facility 35T magnet, Pulsed Facility 65T magnet
Citation: Manuscript in preparation
b
Figure b, Superconducting
upper critical fields as a function of temperature for two samples under pressures of 150 and 170 GPa. Open markers are DC field data and solid ones are pulsed field data. For each sample, we show data for Hc2 (purple and red) and H* (light and dark blue). Solid lines are fits to the formula: Hc2 = Hc2(0)[1-(T/Tc)2].
Inset photos: the diamond anvil cell and the sample.
Superconducting Hydride under Extreme Magnetic Fields and Pressure
S. Mozaffari1, L. Balicas1, V. S. Minkov2, D. Knyazev2, M. I. Eremets2,
M. Einaga3, K. Shimizu3, D. Sun4, F. F. Balakirev4
National High Magnetic Field Laboratory, Florida State University; 2. Max-Planck-Institut fur Chemie;
3. Osaka University; 4. National High Magnetic Field Laboratory, Los Alamos National Laboratory
Funding Grants: G.S. Boebinger (NSF DMR-1157490, NSF DMR-1644779); Balicas (DoE-BES DE-SC0002613); Eremets(ERC- 267777)
Figure a, Resistance as a function of magnetic field at several temperatures (T) for a sulfur hydride sample under hydrostatic pressure of 170 GPa. Red dashed lines Indicate the definition of Hc2, the upper critical magnetic field, and H*, the superconducting transition onset.
a