## Slide 1
Graphene is a unique platform for studying the fractional quantum Hall (FQH) effect, a series of electronic states with excitations that exhibit fractions of an electron charge. In very low disorder devices of monolayer graphene, we report new and unexpected FQH states at Landau level filling ν ± 1/2, but not ± 3/2.
We measured the capacitance of monolayer samples to reveal the presence of insulating FQH states. By sweeping the electron density using electrostatic gates, and applying large perpendicular magnetic fields up to 34T, we observed previously unobserved FQH states which only persist for a narrow range of magnetic fields, and only appear close to charge neutrality. The new FQH states appear at half-filling of a Landau level with either holes or electrons. The appearance of these even-denominator filling FQH states implies a quantum mechanical state with especially exotic properties. We attribute these states to close coupling to the dielectric substrate, consisting of hexagonal boron nitride.
Our work shows the important role the substrate can play in engineering new FQH states in graphene. It inspires new experimental and theoretical work to probe the nature of these unexpected FQH states.
Even denominator fractional quantum Hall states in monolayer graphene
A. Zibrov1, E.M. Spanton1, H. Zhou1, C. Kometter1, T. Taniguchi2, K. Watanabe2, A.F. Young1
1. University of California, Santa Barbara; 2. National Institute for Materials Science
Funding Grants: G.S. Boebinger (NSF DMR-1157490); A.F. Young(NSF DMR-1654186, ARO 69188PHH)
Facilities used: DC Field Facility (Cell 12 Resistive Magnet,
45T Hybrid Magnet)
Citation: A.A. Zibrov, E.M. Spanton, H. Zhou, C. Kometter,
T. Taniguchi, K. Watanabe, A.F. Young, Even-denominator
fractional quantum Hall states at an isospin transition in
monolayer graphene. Nature Physics, 14, 930-935 (2018)
DOI: 10.1038/s41567-018-0190-0
Top: Penetration field capacitance (CP) plotted vs magnetic field (B) and electron density (n0) showing both new and well studied fractional quantum Hall states, which appear as orange and red lines. The two new states are circled in red in the enlarged white dashed box. Bottom: CP vs ν at B = 28.3T, showing dozens of different FQH states, the peaks in CP. Red arrows mark the new FQH states at ± 1/2. Red “X’s” highlight the absence of FQH states at ± 3/2.
CP /c
B (T)
Landau level filling, ν
X
X

## Slide 2
What is the finding? Fractional quantum Hall (FQH) states are insulating states which have excitations that behave like electrons having a fraction of their normal charge. In monolayer graphene, we observed a new and unexpected class of FQH states which occur for a narrow range of magnetic fields around 28 teslas.
Why is this important? Fractional quantum Hall states are one of the most striking effects of electron interactions. Some FQH states exhibit properties which could be used for quantum computation. The unexpected discovery of new FQH states in graphene showcases the potential for engineering new properties due to the tunability of graphene using electric and magnetic fields.
Why did this research need the MagLab? In many samples, the new FQH states only occur for a narrow range of high magnetic fields, up to 30 tesla. Additionally, temperatures below 1 kelvin are required to observe the most fragile of these quantum mechanical states.
Even denominator fractional quantum Hall states in monolayer graphene
A. Zibrov1, E.M. Spanton1, H. Zhou1, C. Kometter1, T. Taniguchi2, K. Watanabe2, A.F. Young1
1. University of California, Santa Barbara; 2. National Institute for Materials Science
Funding Grants: G.S. Boebinger (NSF DMR-1157490); A.F. Young(NSF DMR-1654186, ARO 69188PHH)
Facilities used: DC Field Facility (Cell 12 Resistive Magnet,
45T Hybrid Magnet)
Citation: A.A. Zibrov, E.M. Spanton, H. Zhou, C. Kometter,
T. Taniguchi, K. Watanabe, A.F. Young, Even-denominator
fractional quantum Hall states at an isospin transition in
monolayer graphene. Nature Physics, 14, 930-935 (2018)
DOI: 10.1038/s41567-018-0190-0
Top: Penetration field capacitance (CP) plotted vs magnetic field (B) and electron density (n0) showing both new and well studied fractional quantum Hall states, which appear as orange and red lines. The two new states are circled in red in the enlarged white dashed box. Bottom: CP vs ν at B = 28.3T, showing dozens of different FQH states, the peaks in CP. Red arrows mark the new FQH states at ± 1/2. Red “X’s” highlight the absence of FQH states at ± 3/2.
CP /c
B (T)
Landau level filling, ν
X
X
Notes: 1. What is the finding?
Here to be included a short description in layman language of the finding
2. Why this finding is important?
A short description of why the finding is important for scientific community, technology, society, etc…
3. Why NHMFL?
The answer to this question should provide information on why this finding could be achieved (only) at NHMFL (what unique capability of MagLab was essential for this finding).