## Slide 1
Linear magnetoresistance in a cuprate superconductor
P. Giraldo-Gallo1,2, J.A. Galvis1,3, Z. Stegen1, K.A. Modic4, F.F. Balakirev5, J.B. Betts5, X. Lian1, C. Moir1, S.C. Riggs1, . J. Wu6, A.T. Bollinger6, X.He,6,7, I. Božović6,7, B.J. Ramshaw5,8, R.D. McDonald5, G.S. Boebinger1, A. Shekhter,1
1. National High Magnetic Field Laboratory, Florida State University; 2. Universidad de Los Andes, Bogotá; 3. Universidad Central, Bogotá; 4. Max Planck Institute for Chemical Physics of Solids, Dresden; 5. Los Alamos National Laboratory; 6. Brookhaven National Laboratory; 7. Yale University; 8. Cornell University.
Funding Grants: G.S. Boebinger (NSF DMR-1157490, NSF DMR-1644779); R.D. McDonald (DOE-BES “Science at 100 T”); X. He (Gordon and Betty Moore Foundation’s EPiQS Initiative through grant GBMF4410)
Scale plays an important role in our understanding of conventional metals; band theory provides the framework for describing solids, but it is the band filling, or Fermi energy scale, that dictates the materials’ properties. To date this Fermi-liquid description of metals enables the charge transport in most metals to be described in terms of long-lived electron-like quasi-particles. This work addresses how this description breaks down for the most strongly interacting materials, such as the anomalous –“strange” – metallic state of high temperature superconductors.
Resistance measurements of the cuprate superconductor
La2-xSrxCuO4 in some of our highest available magnetic fields revealed surprising resistivity behavior that is linear in magnetic field, reminiscent of the familiar, but still-unexplained, linear-in-temperature resistivity.
The similar linearity of the resistance in both magnetic field and temperature indicates a completely new mechanism in which the energy-scale of the applied field as well as the thermal energy dictate the resistance, without regard for an internal energy scale of the system such as the Fermi energy. The characterization of this behavior and the connection to quantum criticality, advances our knowledge of the strongly correlated matter that hosts high temperature superconductivity.
B
A Magnetoresistance of optimally doped La2-xSrxCuO4 revealing a saturating field gradient (b) at low temperature. B Linear temperature dependence of the resistance with slope (a), which is found to have the same doping dependence as b.
Facilities and instrumentation used: The 65 T short pulse, 60 T long-pulse, and 100 T magnet systems at the NHMFL Pulsed Field Facility,
Citation: P. Giraldo-Gallo, J.A. Galvis, Z. Stegen, K.A. Modic, F.F. Balakirev, J.B. Betts, X. Lian, C. Moir, S.C. Riggs, J. Wu, A.T. Bollinger, X.He, I. Božović, B.J. Ramshaw, R.D. McDonald, G.S. Boebinger, A. Shekhter, Science 361, 479–481 (2018) DOI: 10.1126/science.aan3178

## Slide 2
Schematic doping-field-temperature (p-B-T) phase diagram in the vicinity of the critical doping pcrit. Note that the superconducting phase surrounding the critical point is not shown. The magenta region in the p-T plane indicates where linear-T resistivity exists. The fan-shaped region of linear-B resistivity in the p-B plane is shaded in blue.
What is the finding? The application of the highest available magnetic fields reveals that, in stark contrast to our understanding of conventional metals, the resistivity of the original high-temperature superconductors – the “cuprates” – scales linearly with both the strength of magnetic field and temperature. By exploring an extended region of temperature, chemical composition (doping) and magnetic field phase-space the connection to an underlying quantum critical point is revealed.
Why is this important? Our understanding of how electrons carry current in the majority of semiconductors and metals enables the design of all modern electronics. However materials with some of the most fascinating and potentially useful properties, like high temperature superconductors, behave differently due to the strong interactions between the electrons. The strong interactions between the electrons are also a major reason that high temperature superconductivity remains poorly understood. By discovering the linear magnetoresistance in the cuprates, we hope to shed light upon what makes this family of materials superconduct at such high temperatures.
Why did this research need the MagLab? Magnetic fields of 50T are required to suppress superconductivity in this material at low temperatures. Much higher fields, of 80T to 100T, are required to provide a sufficient range of magnetic field over which the linearity of magnetoresistance can be determined.
Facilities and instrumentation used: The 65 T short pulse, 60 T long-pulse, and 100 T magnet systems at the NHMFL Pulsed Field Facility,
Citation: P. Giraldo-Gallo, J.A. Galvis, Z. Stegen, K.A. Modic, F.F. Balakirev, J.B. Betts, X. Lian, C. Moir, S.C. Riggs, J. Wu, A.T. Bollinger, X.He, I. Božović, B.J. Ramshaw, R.D. McDonald, G.S. Boebinger, A. Shekhter, Science 361, 479–481 (2018) DOI: 10.1126/science.aan3178
Linear magnetoresistance in a cuprate superconductor
P. Giraldo-Gallo1,2, J.A. Galvis1,3, Z. Stegen1, K.A. Modic4, F.F. Balakirev5, J.B. Betts5, X. Lian1, C. Moir1, S.C. Riggs1, . J. Wu6, A.T. Bollinger6, X.He,6,7, I. Božović6,7, B.J. Ramshaw5,8, R.D. McDonald5, G.S. Boebinger1, A. Shekhter,1
1. National High Magnetic Field Laboratory, Florida State University; 2. Universidad de Los Andes, Bogotá; 3. Universidad Central, Bogotá; 4. Max Planck Institute for Chemical Physics of Solids, Dresden; 5. Los Alamos National Laboratory; 6. Brookhaven National Laboratory; 7. Yale University; 8. Cornell University.
Funding Grants: G.S. Boebinger (NSF DMR-1157490, NSF DMR-1644779); R.D. McDonald (DOE-BES “Science at 100 T”); X. He (Gordon and Betty Moore Foundation’s EPiQS Initiative through grant GBMF4410)