## Slide 1
Restacked-rod-process Nb3Sn superconducting wires will be used in the high-luminosity (HL) upgrade of the Large Hadron Collider particle accelerator at CERN in order to increase the rate of particle collisions. However, the brittle nature of Nb3Sn superconducting wires requires proper of stress and strain management in magnets to be made for the HL-LHC upgrade.
Systematic studies of Nb3Sn axial-strain properties enabled this collaboration to discover the strain irreversibility cliff, an abrupt change of the intrinsic irreversible strain limit  irr,0 , presumably the strain at which cracks start to form in Nb3Sn, as a function of heat-treatment temperature,  , for forming Nb3Sn (see Figure). The strain irreversibility cliff imposes restrictions on the heat treatment that conflict with those required to maintain the conductor’s residual resistivity ratio above 150, as required to ensure stability of magnets against quenching. This collaboration combined studies of strain and residual resistivity ratio properties. These specific measurement capabilities have now permanently relocated from NIST to the MagLab’s Applied Superconductivity Center.
The study led the team to introduce an electro-mechanical stability criterion that takes into account both strain and residual resistivity ratio requirements. It is a valuable tool to inspect Nb3Sn wires before considering them for usage in magnets to achieve optimal cost and performance outcomes.
Instrumentation used: Strain and RRR apparatuses from NIST,
now relocated to Applied Superconductivity Center at the MagLab (ASC-NHMFL). Furnaces at ASC-NHMFL.
Citation: Implications of the strain irreversibility cliff on fabrication of particle-accelerator magnets made of restacked-rod-process Nb3Sn wires N. Cheggour, T. C. Stauffer, W. Starch, L. F. Goodrich, and J. D. Splett, Scientific Reports 9 (2019) 5466. DOI 10.1038/s41598-019-41817-7
Changes proposed to heat-treatment of Large Hadron Collider
Nb3Sn magnets for optimal results
Najib Cheggour1,2,3, Theodore C. Stauffer3, William Starch1, Loren Goodrich2,3, Jolene D. Splett3,
ASC-NHMFL, Florida State University; 2. University of Colorado Boulder; 3. NIST, Boulder Colorado
Funding Grants: DOE/HEP (DE-SC0010690, DE-SC0017657); N. Cheggour. G.S. Boebinger (NSF DMR-1157490, NSF DMR-1644779); W. Starch
Figure: irr,0 ( ) and RRR ( ) dependences for a particular Nb3Sn superconducting wire. Area shaded in gray on the left is where θ is below the cliff onset temperature (determined by the sharp drop in irr,0 ( ) (green). Area shaded in gray on the right is where the residual resistivity ratio (blue) drops below 150. The residual domain between the hatched areas defines the allowable temperature window for an optimal heat treatment. For this wire, the allowable θ of 684 ± 56 °C is very wide.

## Slide 2
What is the finding? When applied to standard superconducting Nb3Sn wires, the electro-mechanical stability criterion required for the Large Hadron Collider upgrade defines a strikingly narrow heat treatment window that is impractical, especially for massive magnets. However, reduced-tin (reduced-Sn) Nb3Sn wires offer a significantly wider heat treatment window that preserves needed strain, resistivity, and superconducting critical current properties (shown in the Figure).
Why is this important? The high-luminosity Large Hadron Collider upgrade will use reduced-Sn Nb3Sn wires of the same design as the wire used in this study. However, the current plan is to conduct heat treatments of magnets at a temperature of 665 C (blue line in Figure). Based on our results, this collaboration is instead proposing that the heat treatment temperature be in the range of 680 to 695 C to ensure that strain-induced degradation of the superconducting critical current remains limited during magnet operation.
Why did this research need the MagLab? The electro-mechanical lab of the ASC-NHMFL (relocated from NIST) has unique measurement capabilities to study strain properties of practical superconductors. The MagLab is the leading U.S. laboratory for these measurements and is one of very few laboratories worldwide capable of performing this specialized electro-mechanical research on superconductors.
Figure: Comparisons of superconducting critical current Ic (0) curves for a particular type of Nb3Sn wire heat-treated for 48 hours at 656, 666, 681, and 695 °C. Samples reacted at 666–695 °C have practically the same Ic values for any given intrinsic strain 0, even beyond irr,0, until the sample reacted at 666 °C starts showing a severe drop of Ic. This drop is more pronounced for the sample reacted at 656 °C, indicating its gradual evolution with lowering temperature θ. The area shaded in gray on the right corresponds to the irreversible strain regime (0 > irr,0) that must be avoided in successful superconducting magnets.
Changes proposed to heat-treatment of Large Hadron Collider
Nb3Sn magnets for optimal results
Najib Cheggour1,2,3, Theodore C. Stauffer3, William Starch1, Loren Goodrich2,3, Jolene D. Splett3,
ASC-NHMFL, Florida State University; 2. University of Colorado Boulder; 3. NIST, Boulder Colorado
Funding Grants: DOE/HEP (DE-SC0010690, DE-SC0017657); N. Cheggour. G.S. Boebinger (NSF DMR-1157490, NSF DMR-1644779); W. Starch
Instrumentation used: Strain and RRR apparatuses from NIST,
now relocated to Applied Superconductivity Center at the MagLab (ASC-NHMFL). Furnaces at ASC-NHMFL.
Citation: Implications of the strain irreversibility cliff on fabrication of particle-accelerator magnets made of restacked-rod-process Nb3Sn wires N. Cheggour, T. C. Stauffer, W. Starch, L. F. Goodrich, and J. D. Splett, Scientific Reports 9 (2019) 5466. DOI 10.1038/s41598-019-41817-7
Notes: 1. What is the finding?
Here to be included a short description in layman language of the finding
2. Why this finding is important?
A short description of why the finding is important for scientific community, technology, society, etc…
3. Why NHMFL?
The answer to this question should provide information on why this finding could be achieved (only) at NHMFL (what unique capability of MagLab was essential for this finding).