## Slide 1
Niobium-Tin, Nb3Sn, conductors are the conductor of choice in high-field magnet applications for nuclear magnetic resonance, accelerators, and fusion. Nb3Sn magnets will be needed for a next-generation (100TeV) proton collider; however, the desired non-Copper current density (Jc) of 1500A/mm2 (at 16T and 4.2K) is substantially above the best presently available Nb3Sn conductor designs.
A variety of variants of Nb3Sn monofilament wires were fabricated in-house at the MagLab to include Nb4Ta rods with Zirconium (Zr) and Hafnium (Hf) additions, both with and without SnO2 suitable for internal oxidation of the Zr and Hf. The properties of the various wires were measured over the entire superconducting range at fields up to 31T at MagLab.
Researchers found that group IV alloying (by Zr and Hf) in the presence of Tantalum (Ta) increases the global vortex pinning force (Layer FP) at 4.2K, more than doubling any previous Nb3Sn production wire (Figure 1). This, in turn, raises the irreversibility field (Hirr) of the wire, thus expanding the magnetic field range over which the superconductor has a zero resistance.
The layer critical current density (Layer Jc) at 16T and 4.2K, exceeds 3500 A/mm2 (Figure 2.), which at the typical 60% fill factor of present high-Jc wires, suggests a non-Copper Jc of 2000 A/mm2, exceeding the goal for the next-generation Future Circular Collider (FCC) planned for CERN.
Facility used: DC Field Facility’s 31T, 50mm Bore Magnet - Cell 7
Citation: S. Balachandran, C. Tarantini, P.J.. Lee, F. Kametani, Y. Su, B. Walker, W.L. Starch, D.C. Larbalestier,
Beneficial influence of Hf and Zr additions to Nb4at%Ta on the vortex pinning of Nb3Sn with and without an O source,
Superconductor Science and Technology, 32, 044006 (2019) doi.org/10.1088/1361-6668/aaff02
Figure 1. Pinning force curves over the full superconducting range indicates a doubling in force magnitude in Hf-based Nb3Sn (blue) over conventional present-day Ta (black) based conductors
Hafnium greatly improves Nb3Sn superconductor for high field magnets
Shreyas Balachandran1, Chiara Tarantini1, Peter J. Lee1, Fumitake Kametani1,2, Yi-Feng Su1,
Benjamin Walker1, William L. Starch1, and David C. Larbalestier1,2
NHMFL, Florida State University; 2. Dept of Mechanical Engineering, Florida State University
Funding Grants: G.S. Boebinger (NSF DMR-1157490, NSF DMR-1644779); DOE (DE-SC0012083 )
Figure 2. Layer critical current density in Hf-based conductors indicate a performance boost of 60% at 16T above the present state-of-the-art Restack Rod Process (RRP) commercial wire.

## Slide 2
What is the finding? MagLab researchers have found that adding the element Hafnium (Hf) to a Niobium (Nb)-Tantalum (Ta) base alloy and forming a superconductor Nb3Sn after reaction with Tin (Sn) at high temperatures of 670°C leads to tremendous improvements in the electrical current carrying ability (Layer Jc) of this conductor wire by 60% at operating magnetic fields of 16T at temperatures of 4.2K (see Figure).
Why is this important? The high increase in the current carrying capacity of superconducting Nb3Sn wire is of particular interest to NMR researchers, MRI clinicians, and scientists pursuing next-generation accelerators and nuclear fusion. In particular, this research result specifically indicates that future 16T dipole magnets for the next-generation Future Circular Collider (FCC) planned to be constructed in CERN can be fabricated using this new Nb3Sn conductor, rather than the riskier high-temperature superconductors.
Why did this research need the MagLab?
The conductor was developed in-house by researchers at the MagLab. In addition, characterization of the conductors at high fields up to the full superconducting range of Nb3Sn (26T) would not have been possible elsewhere.
Figure: Layer critical current density, Jc, in a variety of variants of Nb3Sn monofilament wires fabricated to include Tantalum (Ta), Zirconium (Zr) and Hafnium (Hf) additions, both with and without SnO2 suitable for internal oxidation of the Zr and Hf. Hf based conductors indicate a performance boost above the present state of the art Restack Rod Process (RRP) commercial conductors.
This improvement is nearly 65% at 12T and 60% at 16T.
Hafnium greatly improves Nb3Sn superconductor for high field magnets
Shreyas Balachandran1, Chiara Tarantini1, Peter J. Lee1, Fumitake Kametani1,2, Yi-Feng Su1,
Benjamin Walker1, William L. Starch1, and David C. Larbalestier1,2
NHMFL, Florida State University; 2. Dept of Mechanical Engineering, Florida State University
Funding Grants: G.S. Boebinger (NSF DMR-1157490, NSF DMR-1644779); DOE (DE-SC0012083 )
Facility used: DC Field Facility’s 31T, 50mm Bore Magnet - Cell 7
Citation: S. Balachandran, C. Tarantini, P.J.. Lee, F. Kametani, Y. Su, B. Walker, W.L. Starch, D.C. Larbalestier,
Beneficial influence of Hf and Zr additions to Nb4at%Ta on the vortex pinning of Nb3Sn with and without an O source,
Superconductor Science and Technology, 32, 044006 (2019) doi.org/10.1088/1361-6668/aaff02
Notes: 1. What is the finding?
Here to be included a short description in layman language of the finding
2. Why this finding is important?
A short description of why the finding is important for scientific community, technology, society, etc…
3. Why NHMFL?
The answer to this question should provide information on why this finding could be achieved (only) at NHMFL (what unique capability of MagLab was essential for this finding).