## Slide 1
Figure: A comparison of (a) Hall effect, (b) magnetic torque, and (c) electrical resistivity in the Kondo insulator YbB12 confirms that quantum oscillations and phase transitions show up in all three physical measurements at the same magnetic fields.
This allows phenomena that arise from the coexisting populations of neutral fermions and “conventional” electrons to be identified.
Kondo insulators are a class of electrical insulators in which strong interactions between electrons in different energy levels open up a band gap at low temperatures. YbB12 is a Kondo Insulator that is thought to posses topologically protected quantum states that allow it to display characteristics of both a metal and an insulator.
Using the magnetic fields provided by the 45T Hybrid, 65T pulsed and 73T Duplex magnets, MagLab users measured quantum oscillations and phase transitions in YbB12 in magnetization, resistance and Hall effect. These data revealed the coexistence of relatively ordinary electrons and novel charge-neutral quasiparticles. The surprising suite of observed physical properites results from scattering between the two cohabiting fermion fluids.
The data show that the charge-neutral quasiparticles behave like Fermi-liquid states, responding to magnetic fields in a way resembling that of electrons in regular metals such as copper. On the other hand, the “ordinary” electrons act as a non-Fermi liquid, a groundstate sometimes seen in exotic systems like high-temperature superconductors. These observations verify that a very unusual two-fluid state exists in YbB12, resolving a vexing, five-year-long paradox as to how an insulator can behave like a metal in high magnetic fields and supporting the notion that this constitutes a new phase of matter.
Unconventional Charge Transport in a Kondo Insulator, YbB12
Z. Xiang1,2, K.-W. Chen1, L. Chen1, T. Asaba1,3, Y. Sato3, N. Zhang2, D. Zhang1, Y. Kasahara3, F. Iga4,
W. Coniglio5, Y. Matsuda3, J. Singleton6, Lu Li1,
University of Michigan, 2. University of Science and Technology of China, 3. Kyoto University,
4. Ibaraki University, 5. NHMFL FSU, 6. NHMFL LANL
Funding Grants: Lu Li (NSF DMR-1707620, NSF DMR-2004288, DOE DE-SC0020184) G.S. Boebinger (NSF DMR-1644779)
Facilities and instrumentation used: 45T DC Hybrid magnet, 65T pulsed magnets and the 73T pulsed Duplex magnet.
Citation: Xiang, Z.; Chen, K.; Chen, L.; Asaba, T.; Sato, Y.; Zhang, N.; Zhang, D.; Kasahara, Y.; Iga, F.; Coniglio, W.A.; Matsuda, Y.; Singleton, J.; Li, L., Hall Anomaly, Quantum Oscillations and Possible Lifshitz Transitions in Kondo Insulator YbB12: Evidence for Unconventional Charge Transport, Physical Review X, 12, 021050 (2022) doi.org/10.1103/PhysRevX.12.021050

## Slide 2
What is the finding? Three complementary measurements in intense magnetic fields shed light on a very unusual material that behaves like a metal but does not conduct electricity!
Why is this important? YbB12 is a Kondo insulator, a material that has very poor electrical conductivity at low temperatures. However, astonishingly, the resistance and magnetization of YbB12 oscillate in magnetic fields, behavior usually seen only in metals with very good electrical conductivity. Careful measurements of the resistance and magnetization, compared with measurements of a quantity called the Hall effect, show that the electrons in YbB12 reorganize into two cohabiting fluids.
One fluid behaves in many ways like the electrons in conventional metals; however, this fluid – bizarrely - cannot conduct electrical charge! The other fluid carries electrical charge but acts in a very exotic manner previously seen in materials such as high-temperature superconductors. The properties of YbB12 are due to collisions (“scattering”) among particles from the two fluids, allowing them to interact and influence each others’ behavior. Searches are underway for other materials that host this new phase of matter.
Why did this research need the MagLab? The MagLab has unique magnets that provide the 45–73T magnetic fields essential for the research. MagLab staff worked hard to reduce the electrical noise and mechanical vibrations in the specialized equipment, a crucial ingredient for success with sensitive experiments of this kind.
Unconventional Charge Transport in a Kondo Insulator, YbB12
Z. Xiang1,2, K.-W. Chen1, L. Chen1, T. Asaba1,3, Y. Sato3, N. Zhang2, D. Zhang1, Y. Kasahara3, F. Iga4,
W. Coniglio5, Y. Matsuda3, J. Singleton6, Lu Li1,
University of Michigan, 2. University of Science and Technology of China, 3. Kyoto University,
4. Ibaraki University, 5. NHMFL FSU, 6. NHMFL LANL
Funding Grants: Lu Li (NSF DMR-1707620, NSF DMR-2004288, DOE DE-SC0020184) G.S. Boebinger (NSF DMR-1644779)
Facilities and instrumentation used: 45T DC Hybrid magnet, 65T pulsed
magnets and the 73T pulsed Duplex magnet.
Citation: Xiang, Z.; Chen, K.; Chen, L.; Asaba, T.; Sato, Y.; Zhang, N.; Zhang, D.; Kasahara, Y.; Iga, F.; Coniglio, W.A.; Matsuda, Y.; Singleton, J.; Li, L., Hall Anomaly, Quantum Oscillations and Possible Lifshitz Transitions in Kondo Insulator YbB12: Evidence for Unconventional Charge Transport, Physical Review X, 12, 021050 (2022) doi.org/10.1103/PhysRevX.12.021050
Figure: Sketch of the two fluids in YbB12, showing their densities of states (basically, the number of particles versus energy). On the left are the electrically neutral particles of the first fluid (orange), whose properties oscillate in magnetic fields (shown by the wiggly curve). These particles do not carry electrical current. On the right are particles of the exotic fluid that do conduct electricity (red). Collisions among particles of the two fluids allow the two fluids to influence each other’s behavior; hence the wiggly behavior of the neutral fluid shows up in electrical currents carried by the exotic fluid. This experiment resolves a vexing, five-year-long paradox as to how an insulator can behave like a metal in high magnetic fields.