## Slide 1
SrCu2(BO3)2 is a Mott-Hubbard insulator that hosts an orthogonal spin-dimer system, with a tetragonal unit cell that accommodates spin S = 1/2 Cu2+ dimers arranged in copper-oxygen-boron planes separated by strontium spacer layers. SrCu2(BO3)2 is also a physical realization of the exactly-solvable two-dimensional Shastry-Sutherland model proposed more than four decades ago. The combination of geometrical frustration, exchange interactions that are sensitive to the Cu-O-Cu angle, and proximity to a quantum critical point make this a fascinating compound, very rich in magnetic phases stabilized with tuning parameters such as temperature, external magnetic fields, applied pressures, and disorder induced by chemical substitutions. Thus, SrCu2(BO3)2 is a unique system that provides numerous practical routes to tune exotic states such as spin stripe phases, spin supersolids, spin plaquettes, and quantum spin liquids.
In an effort to understand the extent of the exchange interaction’s dependency on the Cu-O-Cu angle, the user collaboration performed technically difficult magneto-Raman scattering experiments in magnetic fields up to 45T, the highest continuous magnetic field in the world, and coupled these results with first principles calculations. The research team is a diverse group of scientists from Europe and the USA, with the lead author being physics professor at a minority-serving institution who maintains her research laboratory at the MagLab.
The experimental and theoretical work presented here provides a direct correlation between the magnetic interaction and the Cu-O-Cu angle and identifies the phonons that facilitate this interaction between the Cu ions. As such, this work is a milestone in the understanding quantum materials with novel magnetic properties. A clear understanding of the exchange mechanism in these materials is crucial for developing future applications that rely on controllable quantum phenomena.
Magnetoelastic interactions in the spin-dimer compound SrCu2(BO3)2
K. Thirunavukkuarasu1, G. Radtke2, Z. Lu3, M. Lazzeri2, P. C. M. Christianen4, M. V. Ballottin4, H. A. Dabkowska5, B. D. Gaulin5, D. Smirnov3,
M. Jaime6 and A. Saúl7
Florida A&M University; 2. Sorbonne University; 3. National High Magnetic Field Lab; 4. High Field Magnet Laboratory; 5. McMaster University;
6. MagLab, Los Alamos National Laboratory; 7. Aix-Marseille University
Funding Grants: G.S. Boebinger (NSF DMR-2128556); D. Smirnov (DE-FG02-07ER46451); B.D. Gaulin (NSERC Canada); P.C.M. Christianen (HFML-RU/NWO-I)
Facilities and instrumentation used: 45T hybrid magnet system and 31T resistive magnet.
Citation: Thirunavukkuarasu, K.; Radtke, G.; Lu, Z.; Lazzeri, M.; Christianen, P.; Ballottin, M.V.; Dabkowska, H.A.; Gaulin, B.D.; Smirnov, D.; Jaime, M.; Saul, A., Magnetoelastic interactions in SrCu2(BO3)2 studied by Raman scattering experiments and first principles calculations, Physical Review B, 107, 064410 (2023) doi.org/10.1103/PhysRevB.107.064410
1.
2.
Fig.2: (a) Evolution of the energy of four Raman modes of SrCu2(BO3)2 with applied magnetic fields up to 45T. The arrows point to the anomalies detected in 200cm−1 mode coinciding with M/Ms = 1/8, 1/4, and 1/3 phases. (b) Magnetostriction of SrCu2(BO3)2 along a and c axes measured at magnetic fields up to 45T. (c) and (d) Evolution of the 200cm−1 pantograph phonon mode with respect to increasing magnetic fields in the range 24-44T. The data points are shown as open circles and the solid lines are the Lorentzian fit of the data.
Fig.1: Atomic structure of SrCu2(BO3)2 (a) along the [100] direction and (b) along the [001] direction. Sr atoms are in yellow, O in red, B in green, and Cu in blue. The buckling of the [CuBO3]−layers along the [001] direction is visible in (a). The orthogonal Cu dimers have been highlighted in magenta in (b).
(c)
(a)
(b)
Notes: How to compress files size:
On PowerPoint, you can save the attached image (Right click on an image -> Select “Save as picture” -> Then you save the image as PNG). PNG is the image compression without losing the image quality. You replace the original image with the PNG one on PowerPoint. This should reduce the PowerPoint file size.
One thing to be careful about is that you should enlarge your image a bit on PowerPoint before saving so is to avoid losing much resolution.

## Slide 2
What is the finding? Magneto-Raman scattering experiments and first principles calculations show four phonon modes that exhibit strong magnetic field response that mimics the static magnetic properties observed in magnetic fields up to 45T in magnetization and magnetostriction. The observed Raman mode anomalies provide a direct correlation between the magnetic interaction and the Cu-O-Cu angle and identify which particular phonons facilitate this interaction between the Cu ions.
Why is this important? Understanding the nature and origin of magnetic interactions at the microscopic level is extremely important to realize controllable properties in materials for future applications. Magnetic interactions in novel quantum materials involve correlations between electron spins and the crystal lattice. Raman investigations that can reveal the nature of cooperation between the spins and lattice - known as magnetoelastic coupling - are crucial. A thorough understanding of the quantum phenomena that can be stabilized using external agents such as temperature, pressure, electric field and magnetic field will facilitate the development of new technologies and applications in the future.
Why did this research need the MagLab? A typical hurdle in investigating quantum phenomena in any material is accessing the energy scale with the right experimental probe. The energy scale needed to reveal the interaction between the spins and lattice is located at magnetic fields from 15T to 45T. Even though some superconducting magnets offer fields higher than 15T, there is no other laboratory that can offer Raman spectroscopy at continuous magnetic fields up to 45T. Indeed, the MagLab is the laboratory where researchers can perform time-consuming Raman spectroscopy at magnetic fields higher than 30T.
Magnetoelastic interactions in the spin-dimer compound SrCu2(BO3)2
K. Thirunavukkuarasu1, G. Radtke2, Z. Lu3, M. Lazzeri2, P. C. M. Christianen4, M. V. Ballottin4, H. A. Dabkowska5, B. D. Gaulin5, D. Smirnov3,
M. Jaime6 and A. Saúl7
Florida A&M University; 2. Sorbonne University; 3. National High Magnetic Field Lab; 4. High Field Magnet Laboratory; 5. McMaster University;
6. MagLab, Los Alamos National Laboratory; 7. Aix-Marseille University
Funding Grants: G.S. Boebinger (NSF DMR-2128556); D. Smirnov (DE-FG02-07ER46451); B.D. Gaulin (NSERC Canada); P.C.M. Christianen (HFML-RU/NWO-I)
Facilities and instrumentation used: 45T hybrid magnet system and 31T resistive magnet.
Citation: Thirunavukkuarasu, K.; Radtke, G.; Lu, Z.; Lazzeri, M.; Christianen, P.; Ballottin, M.V.; Dabkowska, H.A.; Gaulin, B.D.; Smirnov, D.; Jaime, M.; Saul, A., Magnetoelastic interactions in SrCu2(BO3)2 studied by Raman scattering experiments and first principles calculations, Physical Review B, 107, 064410 (2023) doi.org/10.1103/PhysRevB.107.064410
1.
2.
Fig.2: (a) Evolution of the energy of four Raman modes of SrCu2(BO3)2 with applied magnetic fields up to 45T. The arrows point to the anomalies detected in 200cm−1 mode coinciding with M/Ms = 1/8, 1/4, and 1/3 phases. (b) Magnetostriction of SrCu2(BO3)2 along a and c axes measured at magnetic fields up to 45T. (c) Evolution of the 200cm−1 pantograph phonon mode with respect to increasing magnetic fields in the range 32-44T. The data points are shown as open circles and the solid lines are the Lorentzian fit of the data.
Fig.1: Atomic structure of SrCu2(BO3)2 (a) along the [100] direction and (b) along the [001] direction. Sr atoms are in yellow, O in red, B in green, and Cu in blue. The buckling of the [CuBO3]−layers along the [001] direction is visible in (a). The orthogonal Cu dimers have been highlighted in magenta in (b).
(c)
(a)
(b)
Notes: How to compress files size:
On PowerPoint, you can save the attached image (Right click on an image -> Select “Save as picture” -> Then you save the image as PNG). PNG is the image compression without losing the image quality. You replace the original image with the PNG one on PowerPoint. This should reduce the PowerPoint file size.
One thing to be careful about is that you should enlarge your image a bit on PowerPoint before saving so is to avoid losing much resolution.